|  |  |  |  |  |  | CÔNG TY CỔ PHẦN TƯ VẤN KIỂM ĐỊNH XÂY DỰNG PHÍA NAM SOUTH CONTRUCTION ISPECTION CONSULTANT JSC |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Add: Phòng B01 – Tòa nhà ETUNNEL. L11 - L12 Miếu Nỗi, P. 13, Q. Bình Thạnh, Tp. Hồ Chí Minh. Mobil: (84) 8.35 123 171 – 35 170 334 – Fax: (84)8. 35 123 181. E-mail: scic@dmc.vn |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| NO: 0709-01 |  |  |  | BÁO CÁO KIỂM TRA SIÊU ÂM ULTRASONIC EXAMINATION REPORT |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Page : 01/01 |  |  |  |  |  |  |
| Project: VIETNAM NISSHIN TECHNOMIC PREMIX NEW FACTORY. |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Client: CÔNG TY TNHH QUỐC TẾ VINATA - CHI NHÁNH TP. HỒ CHÍ MINH. |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Test place: CÔNG TY CP CK XD TM ĐẠI DŨNG . |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Test method : AWS D1.1-2015 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Name of sample: JB2 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Date of testing: 08/07/2019 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | # Specification: AWS D1.1-2015 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| KETCH : |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| PREPARATION |  |  |  |  |  |  |  | SURFACE CONDITION |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | COUPLANT |  |  |  |  |  |  |  |  | MATERIAL |  |  |  |  |  |  |  |  |  |  |  |  |  |
| . Single V . Double V . Single V backing . Others |  |  |  |  |  |  |  | . Machined . Ground . Rolled |  |  |  |  |  |  |  |  |  | . One side . Both side . One surface . Both surface |  |  |  |  |  |  |  | . Water . Oil . Grease . Cellulose paste |  |  |  |  |  |  |  | . Carbon steel . Stainless steel |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | . Diameter : . W/ thickness |  |  |  |  |  | 8 |  |  | mm mm |  |  |  |  |
| UT INSTRUMENT |  |  |  |  |  |  |  |  |  |  |  |  |  | PROBE REFERENCE LEVEL |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | CALIBRATION BLOCKS |  |  |  |  |  |  |  |  |  |  |  |  |  |
| .GE USM 35 X DAC 13604a |  |  |  |  |  |  |  |  |  |  |  |  |  | . MSEB 4 00 . SWB 70-2E |  |  |  |  |  | N0 57426-51239 N0 58416-2816 |  |  |  |  |  |  |  | 56 48 |  | dB dB |  |  |  | . V1 – IIW |  |  |  |  |  |  |  |  |  |  |  |  |  |
| #### RESULT |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| #### Name of sample |  | #### Test length, mm | #### Transducer Angle |  | #### Indication N0 |  |  |  |  | #### Leg |  |  | #### Decibel |  |  |  |  |  |  |  |  |  |  |  |  |  | #### Discontinuities |  |  |  |  |  |  |  |  |  |  |  | #### Assess to AWS D1.1:2015 |  |  | #### Remark |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | #### Indication level |  |  |  | #### Reference level |  | #### Attenuation factor |  |  |  | #### Indication rating |  |  |  | #### Length |  | #### Sound Path |  |  |  |  |  | #### Depth from A surface |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | #### a |  |  |  | #### b |  | #### c |  |  |  | #### d |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| #### P1 |  | #### 500 | #### 70 |  | #### - |  |  |  |  | #### - |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  |  |  | #### - |  |  |  | Accept |  |  |  |  |  |  |  |  |
| P2 |  | #### 250 | #### 70 |  | #### - |  |  |  |  | #### - |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  |  |  | #### - |  |  |  | Accept |  |  |  |  |  |  |  |  |
| P3 |  | 250 | #### 70 |  | #### - |  |  |  |  | #### - |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  |  |  | #### - |  |  |  | Accept |  |  |  |  |  |  |  |  |
| P4 |  | 250 | #### 70 |  | #### - |  |  |  |  | #### - |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  |  |  | #### - |  |  |  | Accept |  |  |  |  |  |  |  |  |
| P5 |  | 250 | #### 70 |  | #### - |  |  |  |  | #### - |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  |  |  | #### - |  |  |  | Accept |  |  |  |  |  |  |  |  |
| P6 |  | 250 | #### 70 |  | #### - |  |  |  |  | #### - |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  |  |  | #### - |  |  |  | Accept |  |  |  |  |  |  |  |  |
| Quatest3 12/07/2019 |  |  |  |  |  |  |  |  |  | Tested by |  |  |  |  |  |  |  |  |  |  |  |  | PT. Laboratory |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Vice Director |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  | Đào Công Huân |  |  |  |  |  |  |  |  |  |  |  | Nguyễn Văn Hồng Chi |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Nguyễn Thị Thủy |  |  |  |  |  |  |  |  |
| Name & dated signature |  |  |  |  |  |  |  |  |  | Name & dated signature |  |  |  |  |  |  |  |  |  |  |  |  | Name & dated signature |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Name & dated signature |  |  |  |  |  |  |  |  |  |

|  |  |  |  |  |  | CÔNG TY CỔ PHẦN TƯ VẤN KIỂM ĐỊNH XÂY DỰNG PHÍA NAM SOUTH CONTRUCTION ISPECTION CONSULTANT JSC |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Add: Phòng B01 – Tòa nhà ETUNNEL. L11 - L12 Miếu Nỗi, P. 13, Q. Bình Thạnh, Tp. Hồ Chí Minh. Mobil: (84) 8.35 123 171 – 35 170 334 – Fax: (84)8. 35 123 181. E-mail: scic@dmc.vn |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| NO: 0709-02 |  |  |  | BÁO CÁO KIỂM TRA SIÊU ÂM ULTRASONIC EXAMINATION REPORT |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Page : 01/01 |  |  |  |  |  |  |
| Project: VIETNAM NISSHIN TECHNOMIC PREMIX NEW FACTORY. |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Client: CÔNG TY TNHH QUỐC TẾ VINATA - CHI NHÁNH TP. HỒ CHÍ MINH. |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Test place: CÔNG TY CP CK XD TM ĐẠI DŨNG . |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Test method : AWS D1.1-2015 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Name of sample: JB1 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Date of testing: 08/07/2019 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | # Specification: AWS D1.1-2015 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| KETCH : |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| PREPARATION |  |  |  |  |  |  |  | SURFACE CONDITION |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | COUPLANT |  |  |  |  |  |  |  |  | MATERIAL |  |  |  |  |  |  |  |  |  |  |  |  |  |
| . Single V . Double V . Single V backing . Others |  |  |  |  |  |  |  | . Machined . Ground . Rolled |  |  |  |  |  |  |  |  |  | . One side . Both side . One surface . Both surface |  |  |  |  |  |  |  | . Water . Oil . Grease . Cellulose paste |  |  |  |  |  |  |  | . Carbon steel . Stainless steel |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | . Diameter : . W/ thickness |  |  |  |  |  | 8 |  |  | mm mm |  |  |  |  |
| UT INSTRUMENT |  |  |  |  |  |  |  |  |  |  |  |  |  | PROBE REFERENCE LEVEL |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | CALIBRATION BLOCKS |  |  |  |  |  |  |  |  |  |  |  |  |  |
| .GE USM 35 X DAC 13604a |  |  |  |  |  |  |  |  |  |  |  |  |  | . MSEB 4 00 . SWB 70-2E |  |  |  |  |  | N0 57426-51239 N0 58416-2816 |  |  |  |  |  |  |  | 56 48 |  | dB dB |  |  |  | . V1 – IIW |  |  |  |  |  |  |  |  |  |  |  |  |  |
| #### RESULT |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| #### Name of sample |  | #### Test length, mm | #### Transducer Angle |  | #### Indication N0 |  |  |  |  | #### Leg |  |  | #### Decibel |  |  |  |  |  |  |  |  |  |  |  |  |  | #### Discontinuities |  |  |  |  |  |  |  |  |  |  |  | #### Assess to AWS D1.1:2015 |  |  | #### Remark |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | #### Indication level |  |  |  | #### Reference level |  | #### Attenuation factor |  |  |  | #### Indication rating |  |  |  | #### Length |  | #### Sound Path |  |  |  |  |  | #### Depth from A surface |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | #### a |  |  |  | #### b |  | #### c |  |  |  | #### d |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| #### P1 |  | #### 250 | #### 70 |  | #### - |  |  |  |  | #### - |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  |  |  | #### - |  |  |  | Accept |  |  |  |  |  |  |  |  |
| P2 |  | #### 250 | #### 70 |  | #### - |  |  |  |  | #### - |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  |  |  | #### - |  |  |  | Accept |  |  |  |  |  |  |  |  |
| P3 |  | 250 | #### 70 |  | #### - |  |  |  |  | #### - |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  |  |  | #### - |  |  |  | Accept |  |  |  |  |  |  |  |  |
| P4 |  | 250 | #### 70 |  | #### - |  |  |  |  | #### - |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  |  |  | #### - |  |  |  | Accept |  |  |  |  |  |  |  |  |
| P5 |  | 250 | #### 70 |  | #### - |  |  |  |  | #### - |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  |  |  | #### - |  |  |  | Accept |  |  |  |  |  |  |  |  |
| P6 |  | 250 | #### 70 |  | #### - |  |  |  |  | #### - |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  |  |  | #### - |  |  |  | Accept |  |  |  |  |  |  |  |  |
| Quatest3 12/07/2019 |  |  |  |  |  |  |  |  |  | Tested by |  |  |  |  |  |  |  |  |  |  |  |  | PT. Laboratory |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Vice Director |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  | Đào Công Huân |  |  |  |  |  |  |  |  |  |  |  | Nguyễn Văn Hồng Chi |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Nguyễn Thị Thủy |  |  |  |  |  |  |  |  |
| Name & dated signature |  |  |  |  |  |  |  |  |  | Name & dated signature |  |  |  |  |  |  |  |  |  |  |  |  | Name & dated signature |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Name & dated signature |  |  |  |  |  |  |  |  |  |

|  |  |  |  |  |  | CÔNG TY CỔ PHẦN TƯ VẤN KIỂM ĐỊNH XÂY DỰNG PHÍA NAM SOUTH CONTRUCTION ISPECTION CONSULTANT JSC |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Add: Phòng B01 – Tòa nhà ETUNNEL. L11 - L12 Miếu Nỗi, P. 13, Q. Bình Thạnh, Tp. Hồ Chí Minh. Mobil: (84) 8.35 123 171 – 35 170 334 – Fax: (84)8. 35 123 181. E-mail: scic@dmc.vn |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| NO: 0709-03 |  |  |  | BÁO CÁO KIỂM TRA SIÊU ÂM ULTRASONIC EXAMINATION REPORT |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Page : 01/01 |  |  |  |  |  |  |
| Project: VIETNAM NISSHIN TECHNOMIC PREMIX NEW FACTORY. |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Client: CÔNG TY TNHH QUỐC TẾ VINATA - CHI NHÁNH TP. HỒ CHÍ MINH. |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Test place: CÔNG TY CP CK XD TM ĐẠI DŨNG . |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Test method : AWS D1.1-2015 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Name of sample: AR31 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Date of testing: 08 & 10/07/2019 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | # Specification: AWS D1.1-2015 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| KETCH : |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| PREPARATION |  |  |  |  |  |  |  | SURFACE CONDITION |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | COUPLANT |  |  |  |  |  |  |  |  | MATERIAL |  |  |  |  |  |  |  |  |  |  |  |  |  |
| . Single V . Double V . Single V backing . Others |  |  |  |  |  |  |  | . Machined . Ground . Rolled |  |  |  |  |  |  |  |  |  | . One side . Both side . One surface . Both surface |  |  |  |  |  |  |  | . Water . Oil . Grease . Cellulose paste |  |  |  |  |  |  |  | . Carbon steel . Stainless steel |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | . Diameter : . W/ thickness |  |  |  |  |  | 8 |  |  | mm mm |  |  |  |  |
| UT INSTRUMENT |  |  |  |  |  |  |  |  |  |  |  |  |  | PROBE REFERENCE LEVEL |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | CALIBRATION BLOCKS |  |  |  |  |  |  |  |  |  |  |  |  |  |
| .GE USM 35 X DAC 13604a |  |  |  |  |  |  |  |  |  |  |  |  |  | . MSEB 4 00 . SWB 70-2E |  |  |  |  |  | N0 57426-51239 N0 58416-2816 |  |  |  |  |  |  |  | 56 48 |  | dB dB |  |  |  | . V1 – IIW |  |  |  |  |  |  |  |  |  |  |  |  |  |
| #### RESULT |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| #### Name of sample |  | #### Test length, mm | #### Transducer Angle |  | #### Indication N0 |  |  |  |  | #### Leg |  |  | #### Decibel |  |  |  |  |  |  |  |  |  |  |  |  |  | #### Discontinuities |  |  |  |  |  |  |  |  |  |  |  | #### Assess to AWS D1.1:2015 |  |  | #### Remark |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | #### Indication level |  |  |  | #### Reference level |  | #### Attenuation factor |  |  |  | #### Indication rating |  |  |  | #### Length |  | #### Sound Path |  |  |  |  |  | #### Depth from A surface |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | #### a |  |  |  | #### b |  | #### c |  |  |  | #### d |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| #### P1 |  | #### 330 | #### 70 |  | #### - |  |  |  |  | #### - |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  |  |  | #### - |  |  |  | Accept |  |  |  |  |  |  |  |  |
| P2 |  | #### 165 | #### 70 |  | #### - |  |  |  |  | #### - |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  |  |  | #### - |  |  |  | Accept |  |  |  |  |  |  |  |  |
| P3 |  | 330 | #### 70 |  | #### - |  |  |  |  | #### - |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  |  |  | #### - |  |  |  | Accept |  |  |  |  |  |  |  |  |
| Quatest3 12/07/2019 |  |  |  |  |  |  |  |  |  | Tested by |  |  |  |  |  |  |  |  |  |  |  |  | PT. Laboratory |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Vice Director |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  | Đào Công Huân |  |  |  |  |  |  |  |  |  |  |  | Nguyễn Văn Hồng Chi |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Nguyễn Thị Thủy |  |  |  |  |  |  |  |  |
| Name & dated signature |  |  |  |  |  |  |  |  |  | Name & dated signature |  |  |  |  |  |  |  |  |  |  |  |  | Name & dated signature |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Name & dated signature |  |  |  |  |  |  |  |  |  |

|  |  |  |  |  |  | CÔNG TY CỔ PHẦN TƯ VẤN KIỂM ĐỊNH XÂY DỰNG PHÍA NAM SOUTH CONTRUCTION ISPECTION CONSULTANT JSC |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Add: Phòng B01 – Tòa nhà ETUNNEL. L11 - L12 Miếu Nỗi, P. 13, Q. Bình Thạnh, Tp. Hồ Chí Minh. Mobil: (84) 8.35 123 171 – 35 170 334 – Fax: (84)8. 35 123 181. E-mail: scic@dmc.vn |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| NO: 0709-04 |  |  |  | BÁO CÁO KIỂM TRA SIÊU ÂM ULTRASONIC EXAMINATION REPORT |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Page : 01/01 |  |  |  |  |  |  |
| Project: VIETNAM NISSHIN TECHNOMIC PREMIX NEW FACTORY. |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Client: CÔNG TY TNHH QUỐC TẾ VINATA - CHI NHÁNH TP. HỒ CHÍ MINH. |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Test place: CÔNG TY CP CK XD TM ĐẠI DŨNG . |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Test method : AWS D1.1-2015 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Name of sample: AR30 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Date of testing: 08 & 10/07/2019 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | # Specification: AWS D1.1-2015 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| KETCH : |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| PREPARATION |  |  |  |  |  |  |  | SURFACE CONDITION |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | COUPLANT |  |  |  |  |  |  |  |  | MATERIAL |  |  |  |  |  |  |  |  |  |  |  |  |  |
| . Single V . Double V . Single V backing . Others |  |  |  |  |  |  |  | . Machined . Ground . Rolled |  |  |  |  |  |  |  |  |  | . One side . Both side . One surface . Both surface |  |  |  |  |  |  |  | . Water . Oil . Grease . Cellulose paste |  |  |  |  |  |  |  | . Carbon steel . Stainless steel |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | . Diameter : . W/ thickness |  |  |  |  |  | 8 |  |  | mm mm |  |  |  |  |
| UT INSTRUMENT |  |  |  |  |  |  |  |  |  |  |  |  |  | PROBE REFERENCE LEVEL |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | CALIBRATION BLOCKS |  |  |  |  |  |  |  |  |  |  |  |  |  |
| .GE USM 35 X DAC 13604a |  |  |  |  |  |  |  |  |  |  |  |  |  | . MSEB 4 00 . SWB 70-2E |  |  |  |  |  | N0 57426-51239 N0 58416-2816 |  |  |  |  |  |  |  | 56 48 |  | dB dB |  |  |  | . V1 – IIW |  |  |  |  |  |  |  |  |  |  |  |  |  |
| #### RESULT |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| #### Name of sample |  | #### Test length, mm | #### Transducer Angle |  | #### Indication N0 |  |  |  |  | #### Leg |  |  | #### Decibel |  |  |  |  |  |  |  |  |  |  |  |  |  | #### Discontinuities |  |  |  |  |  |  |  |  |  |  |  | #### Assess to AWS D1.1:2015 |  |  | #### Remark |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | #### Indication level |  |  |  | #### Reference level |  | #### Attenuation factor |  |  |  | #### Indication rating |  |  |  | #### Length |  | #### Sound Path |  |  |  |  |  | #### Depth from A surface |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | #### a |  |  |  | #### b |  | #### c |  |  |  | #### d |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| #### P1 |  | #### 330 | #### 70 |  | #### - |  |  |  |  | #### - |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  |  |  | #### - |  |  |  | Accept |  |  |  |  |  |  |  |  |
| P2 |  | #### 165 | #### 70 |  | #### - |  |  |  |  | #### - |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  |  |  | #### - |  |  |  | Accept |  |  |  |  |  |  |  |  |
| P3 |  | 165 | #### 70 |  | #### - |  |  |  |  | #### - |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  |  |  | #### - |  |  |  | Accept |  |  |  |  |  |  |  |  |
| P4 |  | 165 | #### 70 |  | #### - |  |  |  |  | #### - |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  |  |  | #### - |  |  |  | Accept |  |  |  |  |  |  |  |  |
| P5 |  | 165 | #### 70 |  | #### - |  |  |  |  | #### - |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  |  |  | #### - |  |  |  | Accept |  |  |  |  |  |  |  |  |
| P6 |  | 330 | #### 70 |  | #### - |  |  |  |  | #### - |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  |  |  | #### - |  |  |  | Accept |  |  |  |  |  |  |  |  |
| Quatest3 12/07/2019 |  |  |  |  |  |  |  |  |  | Tested by |  |  |  |  |  |  |  |  |  |  |  |  | PT. Laboratory |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Vice Director |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  | Đào Công Huân |  |  |  |  |  |  |  |  |  |  |  | Nguyễn Văn Hồng Chi |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Nguyễn Thị Thủy |  |  |  |  |  |  |  |  |
| Name & dated signature |  |  |  |  |  |  |  |  |  | Name & dated signature |  |  |  |  |  |  |  |  |  |  |  |  | Name & dated signature |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Name & dated signature |  |  |  |  |  |  |  |  |  |

|  |  |  |  |  |  | CÔNG TY CỔ PHẦN TƯ VẤN KIỂM ĐỊNH XÂY DỰNG PHÍA NAM SOUTH CONTRUCTION ISPECTION CONSULTANT JSC |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Add: Phòng B01 – Tòa nhà ETUNNEL. L11 - L12 Miếu Nỗi, P. 13, Q. Bình Thạnh, Tp. Hồ Chí Minh. Mobil: (84) 8.35 123 171 – 35 170 334 – Fax: (84)8. 35 123 181. E-mail: scic@dmc.vn |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| NO: 0709-05 |  |  |  | BÁO CÁO KIỂM TRA SIÊU ÂM ULTRASONIC EXAMINATION REPORT |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Page : 01/01 |  |  |  |  |  |  |
| Project: VIETNAM NISSHIN TECHNOMIC PREMIX NEW FACTORY. |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Client: CÔNG TY TNHH QUỐC TẾ VINATA - CHI NHÁNH TP. HỒ CHÍ MINH. |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Test place: CÔNG TY CP CK XD TM ĐẠI DŨNG . |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Test method : AWS D1.1-2015 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Name of sample: AR22 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Date of testing: 08 & 10/07/2019 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | # Specification: AWS D1.1-2015 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| KETCH : |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| PREPARATION |  |  |  |  |  |  |  | SURFACE CONDITION |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | COUPLANT |  |  |  |  |  |  |  |  | MATERIAL |  |  |  |  |  |  |  |  |  |  |  |  |  |
| . Single V . Double V . Single V backing . Others |  |  |  |  |  |  |  | . Machined . Ground . Rolled |  |  |  |  |  |  |  |  |  | . One side . Both side . One surface . Both surface |  |  |  |  |  |  |  | . Water . Oil . Grease . Cellulose paste |  |  |  |  |  |  |  | . Carbon steel . Stainless steel |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | . Diameter : . W/ thickness |  |  |  |  |  | 8 |  |  | mm mm |  |  |  |  |
| UT INSTRUMENT |  |  |  |  |  |  |  |  |  |  |  |  |  | PROBE REFERENCE LEVEL |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | CALIBRATION BLOCKS |  |  |  |  |  |  |  |  |  |  |  |  |  |
| .GE USM 35 X DAC 13604a |  |  |  |  |  |  |  |  |  |  |  |  |  | . MSEB 4 00 . SWB 70-2E |  |  |  |  |  | N0 57426-51239 N0 58416-2816 |  |  |  |  |  |  |  | 56 48 |  | dB dB |  |  |  | . V1 – IIW |  |  |  |  |  |  |  |  |  |  |  |  |  |
| #### RESULT |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| #### Name of sample |  | #### Test length, mm | #### Transducer Angle |  | #### Indication N0 |  |  |  |  | #### Leg |  |  | #### Decibel |  |  |  |  |  |  |  |  |  |  |  |  |  | #### Discontinuities |  |  |  |  |  |  |  |  |  |  |  | #### Assess to AWS D1.1:2015 |  |  | #### Remark |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | #### Indication level |  |  |  | #### Reference level |  | #### Attenuation factor |  |  |  | #### Indication rating |  |  |  | #### Length |  | #### Sound Path |  |  |  |  |  | #### Depth from A surface |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | #### a |  |  |  | #### b |  | #### c |  |  |  | #### d |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| #### P1 |  | #### 330 | #### 70 |  | #### - |  |  |  |  | #### - |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  |  |  | #### - |  |  |  | Accept |  |  |  |  |  |  |  |  |
| P2 |  | #### 165 | #### 70 |  | #### - |  |  |  |  | #### - |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  |  |  | #### - |  |  |  | Accept |  |  |  |  |  |  |  |  |
| P3 |  | 165 | #### 70 |  | #### - |  |  |  |  | #### - |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  |  |  | #### - |  |  |  | Accept |  |  |  |  |  |  |  |  |
| P4 |  | 165 | #### 70 |  | #### - |  |  |  |  | #### - |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  |  |  | #### - |  |  |  | Accept |  |  |  |  |  |  |  |  |
| P5 |  | 165 | #### 70 |  | #### - |  |  |  |  | #### - |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  |  |  | #### - |  |  |  | Accept |  |  |  |  |  |  |  |  |
| P6 |  | 330 | #### 70 |  | #### - |  |  |  |  | #### - |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  |  |  | #### - |  |  |  | Accept |  |  |  |  |  |  |  |  |
| Quatest3 12/07/2019 |  |  |  |  |  |  |  |  |  | Tested by |  |  |  |  |  |  |  |  |  |  |  |  | PT. Laboratory |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Vice Director |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  | Đào Công Huân |  |  |  |  |  |  |  |  |  |  |  | Nguyễn Văn Hồng Chi |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Nguyễn Thị Thủy |  |  |  |  |  |  |  |  |
| Name & dated signature |  |  |  |  |  |  |  |  |  | Name & dated signature |  |  |  |  |  |  |  |  |  |  |  |  | Name & dated signature |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Name & dated signature |  |  |  |  |  |  |  |  |  |

|  |  |  |  |  |  | CÔNG TY CỔ PHẦN TƯ VẤN KIỂM ĐỊNH XÂY DỰNG PHÍA NAM SOUTH CONTRUCTION ISPECTION CONSULTANT JSC |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Add: Phòng B01 – Tòa nhà ETUNNEL. L11 - L12 Miếu Nỗi, P. 13, Q. Bình Thạnh, Tp. Hồ Chí Minh. Mobil: (84) 8.35 123 171 – 35 170 334 – Fax: (84)8. 35 123 181. E-mail: scic@dmc.vn |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| NO: 00709-06 |  |  |  | BÁO CÁO KIỂM TRA SIÊU ÂM ULTRASONIC EXAMINATION REPORT |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Page : 01/01 |  |  |  |  |  |  |
| Project: VIETNAM NISSHIN TECHNOMIC PREMIX NEW FACTORY. |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Client: CÔNG TY TNHH QUỐC TẾ VINATA - CHI NHÁNH TP. HỒ CHÍ MINH. |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Test place: CÔNG TY CP CK XD TM ĐẠI DŨNG . |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Test method : AWS D1.1-2015 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Name of sample: AR21 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Date of testing: 08 & 10/07/2019 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | # Specification: AWS D1.1-2015 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| KETCH : |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| PREPARATION |  |  |  |  |  |  |  | SURFACE CONDITION |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | COUPLANT |  |  |  |  |  |  |  |  | MATERIAL |  |  |  |  |  |  |  |  |  |  |  |  |  |
| . Single V . Double V . Single V backing . Others |  |  |  |  |  |  |  | . Machined . Ground . Rolled |  |  |  |  |  |  |  |  |  | . One side . Both side . One surface . Both surface |  |  |  |  |  |  |  | . Water . Oil . Grease . Cellulose paste |  |  |  |  |  |  |  | . Carbon steel . Stainless steel |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | . Diameter : . W/ thickness |  |  |  |  |  | 8 |  |  | mm mm |  |  |  |  |
| UT INSTRUMENT |  |  |  |  |  |  |  |  |  |  |  |  |  | PROBE REFERENCE LEVEL |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | CALIBRATION BLOCKS |  |  |  |  |  |  |  |  |  |  |  |  |  |
| .GE USM 35 X DAC 13604a |  |  |  |  |  |  |  |  |  |  |  |  |  | . MSEB 4 00 . SWB 70-2E |  |  |  |  |  | N0 57426-51239 N0 58416-2816 |  |  |  |  |  |  |  | 56 48 |  | dB dB |  |  |  | . V1 – IIW |  |  |  |  |  |  |  |  |  |  |  |  |  |
| #### RESULT |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| #### Name of sample |  | #### Test length, mm | #### Transducer Angle |  | #### Indication N0 |  |  |  |  | #### Leg |  |  | #### Decibel |  |  |  |  |  |  |  |  |  |  |  |  |  | #### Discontinuities |  |  |  |  |  |  |  |  |  |  |  | #### Assess to AWS D1.1:2015 |  |  | #### Remark |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | #### Indication level |  |  |  | #### Reference level |  | #### Attenuation factor |  |  |  | #### Indication rating |  |  |  | #### Length |  | #### Sound Path |  |  |  |  |  | #### Depth from A surface |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | #### a |  |  |  | #### b |  | #### c |  |  |  | #### d |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| #### P1 |  | #### 330 | #### 70 |  | #### - |  |  |  |  | #### - |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  |  |  | #### - |  |  |  | Accept |  |  |  |  |  |  |  |  |
| P2 |  | #### 165 | #### 70 |  | #### - |  |  |  |  | #### - |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  |  |  | #### - |  |  |  | Accept |  |  |  |  |  |  |  |  |
| P3 |  | 165 | #### 70 |  | #### - |  |  |  |  | #### - |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  |  |  | #### - |  |  |  | Accept |  |  |  |  |  |  |  |  |
| P4 |  | 165 | #### 70 |  | #### - |  |  |  |  | #### - |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  |  |  | #### - |  |  |  | Accept |  |  |  |  |  |  |  |  |
| P5 |  | 165 | #### 70 |  | #### - |  |  |  |  | #### - |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  |  |  | #### - |  |  |  | Accept |  |  |  |  |  |  |  |  |
| P6 |  | 330 | #### 70 |  | #### - |  |  |  |  | #### - |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  |  |  | #### - |  |  |  | Accept |  |  |  |  |  |  |  |  |
| Quatest3 12/07/2019 |  |  |  |  |  |  |  |  |  | Tested by |  |  |  |  |  |  |  |  |  |  |  |  | PT. Laboratory |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Vice Director |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  | Đào Công Huân |  |  |  |  |  |  |  |  |  |  |  | Nguyễn Văn Hồng Chi |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Nguyễn Thị Thủy |  |  |  |  |  |  |  |  |
| Name & dated signature |  |  |  |  |  |  |  |  |  | Name & dated signature |  |  |  |  |  |  |  |  |  |  |  |  | Name & dated signature |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Name & dated signature |  |  |  |  |  |  |  |  |  |

|  |  |  |  |  |  | CÔNG TY CỔ PHẦN TƯ VẤN KIỂM ĐỊNH XÂY DỰNG PHÍA NAM SOUTH CONTRUCTION ISPECTION CONSULTANT JSC |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Add: Phòng B01 – Tòa nhà ETUNNEL. L11 - L12 Miếu Nỗi, P. 13, Q. Bình Thạnh, Tp. Hồ Chí Minh. Mobil: (84) 8.35 123 171 – 35 170 334 – Fax: (84)8. 35 123 181. E-mail: scic@dmc.vn |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| NO: 00709-07 |  |  |  | BÁO CÁO KIỂM TRA SIÊU ÂM ULTRASONIC EXAMINATION REPORT |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Page : 01/01 |  |  |  |  |  |  |
| Project: VIETNAM NISSHIN TECHNOMIC PREMIX NEW FACTORY. |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Client: CÔNG TY TNHH QUỐC TẾ VINATA - CHI NHÁNH TP. HỒ CHÍ MINH. |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Test place: CÔNG TY CP CK XD TM ĐẠI DŨNG . |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Test method : AWS D1.1-2015 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Name of sample: AR21 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Date of testing: 08 & 10/07/2019 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | # Specification: AWS D1.1-2015 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| KETCH : |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| PREPARATION |  |  |  |  |  |  |  | SURFACE CONDITION |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | COUPLANT |  |  |  |  |  |  |  |  | MATERIAL |  |  |  |  |  |  |  |  |  |  |  |  |  |
| . Single V . Double V . Single V backing . Others |  |  |  |  |  |  |  | . Machined . Ground . Rolled |  |  |  |  |  |  |  |  |  | . One side . Both side . One surface . Both surface |  |  |  |  |  |  |  | . Water . Oil . Grease . Cellulose paste |  |  |  |  |  |  |  | . Carbon steel . Stainless steel |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | . Diameter : . W/ thickness |  |  |  |  |  | 8 |  |  | mm mm |  |  |  |  |
| UT INSTRUMENT |  |  |  |  |  |  |  |  |  |  |  |  |  | PROBE REFERENCE LEVEL |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | CALIBRATION BLOCKS |  |  |  |  |  |  |  |  |  |  |  |  |  |
| .GE USM 35 X DAC 13604a |  |  |  |  |  |  |  |  |  |  |  |  |  | . MSEB 4 00 . SWB 70-2E |  |  |  |  |  | N0 57426-51239 N0 58416-2816 |  |  |  |  |  |  |  | 56 48 |  | dB dB |  |  |  | . V1 – IIW |  |  |  |  |  |  |  |  |  |  |  |  |  |
| #### RESULT |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| #### Name of sample |  | #### Test length, mm | #### Transducer Angle |  | #### Indication N0 |  |  |  |  | #### Leg |  |  | #### Decibel |  |  |  |  |  |  |  |  |  |  |  |  |  | #### Discontinuities |  |  |  |  |  |  |  |  |  |  |  | #### Assess to AWS D1.1:2015 |  |  | #### Remark |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | #### Indication level |  |  |  | #### Reference level |  | #### Attenuation factor |  |  |  | #### Indication rating |  |  |  | #### Length |  | #### Sound Path |  |  |  |  |  | #### Depth from A surface |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | #### a |  |  |  | #### b |  | #### c |  |  |  | #### d |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| #### P1 |  | #### 330 | #### 70 |  | #### - |  |  |  |  | #### - |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  |  |  | #### - |  |  |  | Accept |  |  |  |  |  |  |  |  |
| P2 |  | #### 165 | #### 70 |  | #### - |  |  |  |  | #### - |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  |  |  | #### - |  |  |  | Accept |  |  |  |  |  |  |  |  |
| P3 |  | 165 | #### 70 |  | #### - |  |  |  |  | #### - |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  |  |  | #### - |  |  |  | Accept |  |  |  |  |  |  |  |  |
| P4 |  | 165 | #### 70 |  | #### - |  |  |  |  | #### - |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  |  |  | #### - |  |  |  | Accept |  |  |  |  |  |  |  |  |
| P5 |  | 165 | #### 70 |  | #### - |  |  |  |  | #### - |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  |  |  | #### - |  |  |  | Accept |  |  |  |  |  |  |  |  |
| P6 |  | 330 | #### 70 |  | #### - |  |  |  |  | #### - |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  |  |  | #### - |  |  |  | Accept |  |  |  |  |  |  |  |  |
| Quatest3 12/07/2019 |  |  |  |  |  |  |  |  |  | Tested by |  |  |  |  |  |  |  |  |  |  |  |  | PT. Laboratory |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Vice Director |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  | Đào Công Huân |  |  |  |  |  |  |  |  |  |  |  | Nguyễn Văn Hồng Chi |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Nguyễn Thị Thủy |  |  |  |  |  |  |  |  |
| Name & dated signature |  |  |  |  |  |  |  |  |  | Name & dated signature |  |  |  |  |  |  |  |  |  |  |  |  | Name & dated signature |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Name & dated signature |  |  |  |  |  |  |  |  |  |

|  |  |  |  |  |  | CÔNG TY CỔ PHẦN TƯ VẤN KIỂM ĐỊNH XÂY DỰNG PHÍA NAM SOUTH CONTRUCTION ISPECTION CONSULTANT JSC |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Add: Phòng B01 – Tòa nhà ETUNNEL. L11 - L12 Miếu Nỗi, P. 13, Q. Bình Thạnh, Tp. Hồ Chí Minh. Mobil: (84) 8.35 123 171 – 35 170 334 – Fax: (84)8. 35 123 181. E-mail: scic@dmc.vn |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| NO: 00709-08 |  |  |  | BÁO CÁO KIỂM TRA SIÊU ÂM ULTRASONIC EXAMINATION REPORT |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Page : 01/01 |  |  |  |  |  |  |
| Project: VIETNAM NISSHIN TECHNOMIC PREMIX NEW FACTORY. |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Client: CÔNG TY TNHH QUỐC TẾ VINATA - CHI NHÁNH TP. HỒ CHÍ MINH. |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Test place: CÔNG TY CP CK XD TM ĐẠI DŨNG . |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Test method : AWS D1.1-2015 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Name of sample: AR20 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Date of testing: 08 & 10/07/2019 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | # Specification: AWS D1.1-2015 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| KETCH : |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| PREPARATION |  |  |  |  |  |  |  | SURFACE CONDITION |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | COUPLANT |  |  |  |  |  |  |  |  | MATERIAL |  |  |  |  |  |  |  |  |  |  |  |  |  |
| . Single V . Double V . Single V backing . Others |  |  |  |  |  |  |  | . Machined . Ground . Rolled |  |  |  |  |  |  |  |  |  | . One side . Both side . One surface . Both surface |  |  |  |  |  |  |  | . Water . Oil . Grease . Cellulose paste |  |  |  |  |  |  |  | . Carbon steel . Stainless steel |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | . Diameter : . W/ thickness |  |  |  |  |  | 8 |  |  | mm mm |  |  |  |  |
| UT INSTRUMENT |  |  |  |  |  |  |  |  |  |  |  |  |  | PROBE REFERENCE LEVEL |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | CALIBRATION BLOCKS |  |  |  |  |  |  |  |  |  |  |  |  |  |
| .GE USM 35 X DAC 13604a |  |  |  |  |  |  |  |  |  |  |  |  |  | . MSEB 4 00 . SWB 70-2E |  |  |  |  |  | N0 57426-51239 N0 58416-2816 |  |  |  |  |  |  |  | 56 48 |  | dB dB |  |  |  | . V1 – IIW |  |  |  |  |  |  |  |  |  |  |  |  |  |
| #### RESULT |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| #### Name of sample |  | #### Test length, mm | #### Transducer Angle |  | #### Indication N0 |  |  |  |  | #### Leg |  |  | #### Decibel |  |  |  |  |  |  |  |  |  |  |  |  |  | #### Discontinuities |  |  |  |  |  |  |  |  |  |  |  | #### Assess to AWS D1.1:2015 |  |  | #### Remark |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | #### Indication level |  |  |  | #### Reference level |  | #### Attenuation factor |  |  |  | #### Indication rating |  |  |  | #### Length |  | #### Sound Path |  |  |  |  |  | #### Depth from A surface |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | #### a |  |  |  | #### b |  | #### c |  |  |  | #### d |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| #### P1 |  | #### 330 | #### 70 |  | #### - |  |  |  |  | #### - |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  |  |  | #### - |  |  |  | Accept |  |  |  |  |  |  |  |  |
| P2 |  | #### 165 | #### 70 |  | #### - |  |  |  |  | #### - |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  |  |  | #### - |  |  |  | Accept |  |  |  |  |  |  |  |  |
| P3 |  | 165 | #### 70 |  | #### - |  |  |  |  | #### - |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  |  |  | #### - |  |  |  | Accept |  |  |  |  |  |  |  |  |
| P4 |  | 165 | #### 70 |  | #### - |  |  |  |  | #### - |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  |  |  | #### - |  |  |  | Accept |  |  |  |  |  |  |  |  |
| P5 |  | 165 | #### 70 |  | #### - |  |  |  |  | #### - |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  |  |  | #### - |  |  |  | Accept |  |  |  |  |  |  |  |  |
| P6 |  | 330 | #### 70 |  | #### - |  |  |  |  | #### - |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  |  |  | #### - |  |  |  | Accept |  |  |  |  |  |  |  |  |
| Quatest3 12/07/2019 |  |  |  |  |  |  |  |  |  | Tested by |  |  |  |  |  |  |  |  |  |  |  |  | PT. Laboratory |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Vice Director |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  | Đào Công Huân |  |  |  |  |  |  |  |  |  |  |  | Nguyễn Văn Hồng Chi |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Nguyễn Thị Thủy |  |  |  |  |  |  |  |  |
| Name & dated signature |  |  |  |  |  |  |  |  |  | Name & dated signature |  |  |  |  |  |  |  |  |  |  |  |  | Name & dated signature |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Name & dated signature |  |  |  |  |  |  |  |  |  |

|  |  |  |  |  |  | CÔNG TY CỔ PHẦN TƯ VẤN KIỂM ĐỊNH XÂY DỰNG PHÍA NAM SOUTH CONTRUCTION ISPECTION CONSULTANT JSC |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Add: Phòng B01 – Tòa nhà ETUNNEL. L11 - L12 Miếu Nỗi, P. 13, Q. Bình Thạnh, Tp. Hồ Chí Minh. Mobil: (84) 8.35 123 171 – 35 170 334 – Fax: (84)8. 35 123 181. E-mail: scic@dmc.vn |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| NO: 00709-09 |  |  |  | BÁO CÁO KIỂM TRA SIÊU ÂM ULTRASONIC EXAMINATION REPORT |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Page : 01/01 |  |  |  |  |  |  |
| Project: VIETNAM NISSHIN TECHNOMIC PREMIX NEW FACTORY. |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Client: CÔNG TY TNHH QUỐC TẾ VINATA - CHI NHÁNH TP. HỒ CHÍ MINH. |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Test place: CÔNG TY CP CK XD TM ĐẠI DŨNG . |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Test method : AWS D1.1-2015 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Name of sample: AR19 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Date of testing: 08 & 10/07/2019 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | # Specification: AWS D1.1-2015 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| KETCH : |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| PREPARATION |  |  |  |  |  |  |  | SURFACE CONDITION |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | COUPLANT |  |  |  |  |  |  |  |  | MATERIAL |  |  |  |  |  |  |  |  |  |  |  |  |  |
| . Single V . Double V . Single V backing . Others |  |  |  |  |  |  |  | . Machined . Ground . Rolled |  |  |  |  |  |  |  |  |  | . One side . Both side . One surface . Both surface |  |  |  |  |  |  |  | . Water . Oil . Grease . Cellulose paste |  |  |  |  |  |  |  | . Carbon steel . Stainless steel |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | . Diameter : . W/ thickness |  |  |  |  |  | 8 |  |  | mm mm |  |  |  |  |
| UT INSTRUMENT |  |  |  |  |  |  |  |  |  |  |  |  |  | PROBE REFERENCE LEVEL |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | CALIBRATION BLOCKS |  |  |  |  |  |  |  |  |  |  |  |  |  |
| .GE USM 35 X DAC 13604a |  |  |  |  |  |  |  |  |  |  |  |  |  | . MSEB 4 00 . SWB 70-2E |  |  |  |  |  | N0 57426-51239 N0 58416-2816 |  |  |  |  |  |  |  | 56 48 |  | dB dB |  |  |  | . V1 – IIW |  |  |  |  |  |  |  |  |  |  |  |  |  |
| #### RESULT |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| #### Name of sample |  | #### Test length, mm | #### Transducer Angle |  | #### Indication N0 |  |  |  |  | #### Leg |  |  | #### Decibel |  |  |  |  |  |  |  |  |  |  |  |  |  | #### Discontinuities |  |  |  |  |  |  |  |  |  |  |  | #### Assess to AWS D1.1:2015 |  |  | #### Remark |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | #### Indication level |  |  |  | #### Reference level |  | #### Attenuation factor |  |  |  | #### Indication rating |  |  |  | #### Length |  | #### Sound Path |  |  |  |  |  | #### Depth from A surface |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | #### a |  |  |  | #### b |  | #### c |  |  |  | #### d |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| #### P1 |  | #### 330 | #### 70 |  | #### - |  |  |  |  | #### - |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  |  |  | #### - |  |  |  | Accept |  |  |  |  |  |  |  |  |
| P2 |  | #### 165 | #### 70 |  | #### - |  |  |  |  | #### - |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  |  |  | #### - |  |  |  | Accept |  |  |  |  |  |  |  |  |
| P3 |  | 165 | #### 70 |  | #### - |  |  |  |  | #### - |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  |  |  | #### - |  |  |  | Accept |  |  |  |  |  |  |  |  |
| P4 |  | 165 | #### 70 |  | #### - |  |  |  |  | #### - |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  |  |  | #### - |  |  |  | Accept |  |  |  |  |  |  |  |  |
| P5 |  | 165 | #### 70 |  | #### - |  |  |  |  | #### - |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  |  |  | #### - |  |  |  | Accept |  |  |  |  |  |  |  |  |
| P6 |  | 330 | #### 70 |  | #### - |  |  |  |  | #### - |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  |  |  | #### - |  |  |  | Accept |  |  |  |  |  |  |  |  |
| Quatest3 12/07/2019 |  |  |  |  |  |  |  |  |  | Tested by |  |  |  |  |  |  |  |  |  |  |  |  | PT. Laboratory |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Vice Director |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  | Đào Công Huân |  |  |  |  |  |  |  |  |  |  |  | Nguyễn Văn Hồng Chi |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Nguyễn Thị Thủy |  |  |  |  |  |  |  |  |
| Name & dated signature |  |  |  |  |  |  |  |  |  | Name & dated signature |  |  |  |  |  |  |  |  |  |  |  |  | Name & dated signature |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Name & dated signature |  |  |  |  |  |  |  |  |  |

|  |  |  |  |  |  | CÔNG TY CỔ PHẦN TƯ VẤN KIỂM ĐỊNH XÂY DỰNG PHÍA NAM SOUTH CONTRUCTION ISPECTION CONSULTANT JSC |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Add: Phòng B01 – Tòa nhà ETUNNEL. L11 - L12 Miếu Nỗi, P. 13, Q. Bình Thạnh, Tp. Hồ Chí Minh. Mobil: (84) 8.35 123 171 – 35 170 334 – Fax: (84)8. 35 123 181. E-mail: scic@dmc.vn |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| NO: 00709-10 |  |  |  | BÁO CÁO KIỂM TRA SIÊU ÂM ULTRASONIC EXAMINATION REPORT |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Page : 01/01 |  |  |  |  |  |  |
| Project: VIETNAM NISSHIN TECHNOMIC PREMIX NEW FACTORY. |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Client: CÔNG TY TNHH QUỐC TẾ VINATA - CHI NHÁNH TP. HỒ CHÍ MINH. |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Test place: CÔNG TY CP CK XD TM ĐẠI DŨNG . |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Test method : AWS D1.1-2015 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Name of sample: AR18 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Date of testing: 08 & 10/07/2019 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | # Specification: AWS D1.1-2015 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| KETCH : |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| PREPARATION |  |  |  |  |  |  |  | SURFACE CONDITION |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | COUPLANT |  |  |  |  |  |  |  |  | MATERIAL |  |  |  |  |  |  |  |  |  |  |  |  |  |
| . Single V . Double V . Single V backing . Others |  |  |  |  |  |  |  | . Machined . Ground . Rolled |  |  |  |  |  |  |  |  |  | . One side . Both side . One surface . Both surface |  |  |  |  |  |  |  | . Water . Oil . Grease . Cellulose paste |  |  |  |  |  |  |  | . Carbon steel . Stainless steel |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | . Diameter : . W/ thickness |  |  |  |  |  | 8 |  |  | mm mm |  |  |  |  |
| UT INSTRUMENT |  |  |  |  |  |  |  |  |  |  |  |  |  | PROBE REFERENCE LEVEL |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | CALIBRATION BLOCKS |  |  |  |  |  |  |  |  |  |  |  |  |  |
| .GE USM 35 X DAC 13604a |  |  |  |  |  |  |  |  |  |  |  |  |  | . MSEB 4 00 . SWB 70-2E |  |  |  |  |  | N0 57426-51239 N0 58416-2816 |  |  |  |  |  |  |  | 56 48 |  | dB dB |  |  |  | . V1 – IIW |  |  |  |  |  |  |  |  |  |  |  |  |  |
| #### RESULT |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| #### Name of sample |  | #### Test length, mm | #### Transducer Angle |  | #### Indication N0 |  |  |  |  | #### Leg |  |  | #### Decibel |  |  |  |  |  |  |  |  |  |  |  |  |  | #### Discontinuities |  |  |  |  |  |  |  |  |  |  |  | #### Assess to AWS D1.1:2015 |  |  | #### Remark |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | #### Indication level |  |  |  | #### Reference level |  | #### Attenuation factor |  |  |  | #### Indication rating |  |  |  | #### Length |  | #### Sound Path |  |  |  |  |  | #### Depth from A surface |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | #### a |  |  |  | #### b |  | #### c |  |  |  | #### d |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| #### P1 |  | #### 330 | #### 70 |  | #### - |  |  |  |  | #### - |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  |  |  | #### - |  |  |  | Accept |  |  |  |  |  |  |  |  |
| P2 |  | #### 165 | #### 70 |  | #### - |  |  |  |  | #### - |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  |  |  | #### - |  |  |  | Accept |  |  |  |  |  |  |  |  |
| P3 |  | 165 | #### 70 |  | #### - |  |  |  |  | #### - |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  |  |  | #### - |  |  |  | Accept |  |  |  |  |  |  |  |  |
| P4 |  | 165 | #### 70 |  | #### - |  |  |  |  | #### - |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  |  |  | #### - |  |  |  | Accept |  |  |  |  |  |  |  |  |
| P5 |  | 165 | #### 70 |  | #### - |  |  |  |  | #### - |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  |  |  | #### - |  |  |  | Accept |  |  |  |  |  |  |  |  |
| P6 |  | 330 | #### 70 |  | #### - |  |  |  |  | #### - |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  |  |  | #### - |  |  |  | Accept |  |  |  |  |  |  |  |  |
| Quatest3 12/07/2019 |  |  |  |  |  |  |  |  |  | Tested by |  |  |  |  |  |  |  |  |  |  |  |  | PT. Laboratory |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Vice Director |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  | Đào Công Huân |  |  |  |  |  |  |  |  |  |  |  | Nguyễn Văn Hồng Chi |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Nguyễn Thị Thủy |  |  |  |  |  |  |  |  |
| Name & dated signature |  |  |  |  |  |  |  |  |  | Name & dated signature |  |  |  |  |  |  |  |  |  |  |  |  | Name & dated signature |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Name & dated signature |  |  |  |  |  |  |  |  |  |

|  |  |  |  |  |  | CÔNG TY CỔ PHẦN TƯ VẤN KIỂM ĐỊNH XÂY DỰNG PHÍA NAM SOUTH CONTRUCTION ISPECTION CONSULTANT JSC |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Add: Phòng B01 – Tòa nhà ETUNNEL. L11 - L12 Miếu Nỗi, P. 13, Q. Bình Thạnh, Tp. Hồ Chí Minh. Mobil: (84) 8.35 123 171 – 35 170 334 – Fax: (84)8. 35 123 181. E-mail: scic@dmc.vn |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| NO: 00709-11 |  |  |  | BÁO CÁO KIỂM TRA SIÊU ÂM ULTRASONIC EXAMINATION REPORT |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Page : 01/01 |  |  |  |  |  |  |
| Project: VIETNAM NISSHIN TECHNOMIC PREMIX NEW FACTORY. |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Client: CÔNG TY TNHH QUỐC TẾ VINATA - CHI NHÁNH TP. HỒ CHÍ MINH. |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Test place: CÔNG TY CP CK XD TM ĐẠI DŨNG . |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Test method : AWS D1.1-2015 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Name of sample: AR17 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Date of testing: 08 & 10/07/2019 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | # Specification: AWS D1.1-2015 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| KETCH : |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| PREPARATION |  |  |  |  |  |  |  | SURFACE CONDITION |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | COUPLANT |  |  |  |  |  |  |  |  | MATERIAL |  |  |  |  |  |  |  |  |  |  |  |  |  |
| . Single V . Double V . Single V backing . Others |  |  |  |  |  |  |  | . Machined . Ground . Rolled |  |  |  |  |  |  |  |  |  | . One side . Both side . One surface . Both surface |  |  |  |  |  |  |  | . Water . Oil . Grease . Cellulose paste |  |  |  |  |  |  |  | . Carbon steel . Stainless steel |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | . Diameter : . W/ thickness |  |  |  |  |  | 8 |  |  | mm mm |  |  |  |  |
| UT INSTRUMENT |  |  |  |  |  |  |  |  |  |  |  |  |  | PROBE REFERENCE LEVEL |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | CALIBRATION BLOCKS |  |  |  |  |  |  |  |  |  |  |  |  |  |
| .GE USM 35 X DAC 13604a |  |  |  |  |  |  |  |  |  |  |  |  |  | . MSEB 4 00 . SWB 70-2E |  |  |  |  |  | N0 57426-51239 N0 58416-2816 |  |  |  |  |  |  |  | 56 48 |  | dB dB |  |  |  | . V1 – IIW |  |  |  |  |  |  |  |  |  |  |  |  |  |
| #### RESULT |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| #### Name of sample |  | #### Test length, mm | #### Transducer Angle |  | #### Indication N0 |  |  |  |  | #### Leg |  |  | #### Decibel |  |  |  |  |  |  |  |  |  |  |  |  |  | #### Discontinuities |  |  |  |  |  |  |  |  |  |  |  | #### Assess to AWS D1.1:2015 |  |  | #### Remark |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | #### Indication level |  |  |  | #### Reference level |  | #### Attenuation factor |  |  |  | #### Indication rating |  |  |  | #### Length |  | #### Sound Path |  |  |  |  |  | #### Depth from A surface |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | #### a |  |  |  | #### b |  | #### c |  |  |  | #### d |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| #### P1 |  | #### 330 | #### 70 |  | #### - |  |  |  |  | #### - |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  |  |  | #### - |  |  |  | Accept |  |  |  |  |  |  |  |  |
| P2 |  | #### 165 | #### 70 |  | #### - |  |  |  |  | #### - |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  |  |  | #### - |  |  |  | Accept |  |  |  |  |  |  |  |  |
| P3 |  | 165 | #### 70 |  | #### - |  |  |  |  | #### - |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  |  |  | #### - |  |  |  | Accept |  |  |  |  |  |  |  |  |
| P4 |  | 165 | #### 70 |  | #### - |  |  |  |  | #### - |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  |  |  | #### - |  |  |  | Accept |  |  |  |  |  |  |  |  |
| P5 |  | 165 | #### 70 |  | #### - |  |  |  |  | #### - |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  |  |  | #### - |  |  |  | Accept |  |  |  |  |  |  |  |  |
| P6 |  | 330 | #### 70 |  | #### - |  |  |  |  | #### - |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  |  |  | #### - |  |  |  | Accept |  |  |  |  |  |  |  |  |
| Quatest3 12/07/2019 |  |  |  |  |  |  |  |  |  | Tested by |  |  |  |  |  |  |  |  |  |  |  |  | PT. Laboratory |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Vice Director |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  | Đào Công Huân |  |  |  |  |  |  |  |  |  |  |  | Nguyễn Văn Hồng Chi |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Nguyễn Thị Thủy |  |  |  |  |  |  |  |  |
| Name & dated signature |  |  |  |  |  |  |  |  |  | Name & dated signature |  |  |  |  |  |  |  |  |  |  |  |  | Name & dated signature |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Name & dated signature |  |  |  |  |  |  |  |  |  |

|  |  |  |  |  |  | CÔNG TY CỔ PHẦN TƯ VẤN KIỂM ĐỊNH XÂY DỰNG PHÍA NAM SOUTH CONTRUCTION ISPECTION CONSULTANT JSC |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Add: Phòng B01 – Tòa nhà ETUNNEL. L11 - L12 Miếu Nỗi, P. 13, Q. Bình Thạnh, Tp. Hồ Chí Minh. Mobil: (84) 8.35 123 171 – 35 170 334 – Fax: (84)8. 35 123 181. E-mail: scic@dmc.vn |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| NO: 00709-12 |  |  |  | BÁO CÁO KIỂM TRA SIÊU ÂM ULTRASONIC EXAMINATION REPORT |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Page : 01/01 |  |  |  |  |  |  |
| Project: VIETNAM NISSHIN TECHNOMIC PREMIX NEW FACTORY. |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Client: CÔNG TY TNHH QUỐC TẾ VINATA - CHI NHÁNH TP. HỒ CHÍ MINH. |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Test place: CÔNG TY CP CK XD TM ĐẠI DŨNG . |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Test method : AWS D1.1-2015 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Name of sample: AR11/1 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Date of testing: 08 & 10/07/2019 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | # Specification: AWS D1.1-2015 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| KETCH : |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| PREPARATION |  |  |  |  |  |  |  | SURFACE CONDITION |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | COUPLANT |  |  |  |  |  |  |  |  | MATERIAL |  |  |  |  |  |  |  |  |  |  |  |  |  |
| . Single V . Double V . Single V backing . Others |  |  |  |  |  |  |  | . Machined . Ground . Rolled |  |  |  |  |  |  |  |  |  | . One side . Both side . One surface . Both surface |  |  |  |  |  |  |  | . Water . Oil . Grease . Cellulose paste |  |  |  |  |  |  |  | . Carbon steel . Stainless steel |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | . Diameter : . W/ thickness |  |  |  |  |  | 8 |  |  | mm mm |  |  |  |  |
| UT INSTRUMENT |  |  |  |  |  |  |  |  |  |  |  |  |  | PROBE REFERENCE LEVEL |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | CALIBRATION BLOCKS |  |  |  |  |  |  |  |  |  |  |  |  |  |
| .GE USM 35 X DAC 13604a |  |  |  |  |  |  |  |  |  |  |  |  |  | . MSEB 4 00 . SWB 70-2E |  |  |  |  |  | N0 57426-51239 N0 58416-2816 |  |  |  |  |  |  |  | 56 48 |  | dB dB |  |  |  | . V1 – IIW |  |  |  |  |  |  |  |  |  |  |  |  |  |
| #### RESULT |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| #### Name of sample |  | #### Test length, mm | #### Transducer Angle |  | #### Indication N0 |  |  |  |  | #### Leg |  |  | #### Decibel |  |  |  |  |  |  |  |  |  |  |  |  |  | #### Discontinuities |  |  |  |  |  |  |  |  |  |  |  | #### Assess to AWS D1.1:2015 |  |  | #### Remark |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | #### Indication level |  |  |  | #### Reference level |  | #### Attenuation factor |  |  |  | #### Indication rating |  |  |  | #### Length |  | #### Sound Path |  |  |  |  |  | #### Depth from A surface |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | #### a |  |  |  | #### b |  | #### c |  |  |  | #### d |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| #### P1 |  | #### 330 | #### 70 |  | #### - |  |  |  |  | #### - |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  |  |  | #### - |  |  |  | Accept |  |  |  |  |  |  |  |  |
| P2 |  | #### 165 | #### 70 |  | #### - |  |  |  |  | #### - |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  |  |  | #### - |  |  |  | Accept |  |  |  |  |  |  |  |  |
| P3 |  | 165 | #### 70 |  | #### - |  |  |  |  | #### - |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  |  |  | #### - |  |  |  | Accept |  |  |  |  |  |  |  |  |
| P4 |  | 330 | #### 70 |  | #### - |  |  |  |  | #### - |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  |  |  | #### - |  |  |  | Accept |  |  |  |  |  |  |  |  |
| Quatest3 12/07/2019 |  |  |  |  |  |  |  |  |  | Tested by |  |  |  |  |  |  |  |  |  |  |  |  | PT. Laboratory |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Vice Director |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  | Đào Công Huân |  |  |  |  |  |  |  |  |  |  |  | Nguyễn Văn Hồng Chi |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Nguyễn Thị Thủy |  |  |  |  |  |  |  |  |
| Name & dated signature |  |  |  |  |  |  |  |  |  | Name & dated signature |  |  |  |  |  |  |  |  |  |  |  |  | Name & dated signature |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Name & dated signature |  |  |  |  |  |  |  |  |  |

|  |  |  |  |  |  | CÔNG TY CỔ PHẦN TƯ VẤN KIỂM ĐỊNH XÂY DỰNG PHÍA NAM SOUTH CONTRUCTION ISPECTION CONSULTANT JSC |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Add: Phòng B01 – Tòa nhà ETUNNEL. L11 - L12 Miếu Nỗi, P. 13, Q. Bình Thạnh, Tp. Hồ Chí Minh. Mobil: (84) 8.35 123 171 – 35 170 334 – Fax: (84)8. 35 123 181. E-mail: scic@dmc.vn |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| NO: 00709-13 |  |  |  | BÁO CÁO KIỂM TRA SIÊU ÂM ULTRASONIC EXAMINATION REPORT |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Page : 01/01 |  |  |  |  |  |  |
| Project: VIETNAM NISSHIN TECHNOMIC PREMIX NEW FACTORY. |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Client: CÔNG TY TNHH QUỐC TẾ VINATA - CHI NHÁNH TP. HỒ CHÍ MINH. |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Test place: CÔNG TY CP CK XD TM ĐẠI DŨNG . |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Test method : AWS D1.1-2015 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Name of sample: AR11/2 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Date of testing: 08 & 10/07/2019 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | # Specification: AWS D1.1-2015 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| KETCH : |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| PREPARATION |  |  |  |  |  |  |  | SURFACE CONDITION |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | COUPLANT |  |  |  |  |  |  |  |  | MATERIAL |  |  |  |  |  |  |  |  |  |  |  |  |  |
| . Single V . Double V . Single V backing . Others |  |  |  |  |  |  |  | . Machined . Ground . Rolled |  |  |  |  |  |  |  |  |  | . One side . Both side . One surface . Both surface |  |  |  |  |  |  |  | . Water . Oil . Grease . Cellulose paste |  |  |  |  |  |  |  | . Carbon steel . Stainless steel |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | . Diameter : . W/ thickness |  |  |  |  |  | 8 |  |  | mm mm |  |  |  |  |
| UT INSTRUMENT |  |  |  |  |  |  |  |  |  |  |  |  |  | PROBE REFERENCE LEVEL |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | CALIBRATION BLOCKS |  |  |  |  |  |  |  |  |  |  |  |  |  |
| .GE USM 35 X DAC 13604a |  |  |  |  |  |  |  |  |  |  |  |  |  | . MSEB 4 00 . SWB 70-2E |  |  |  |  |  | N0 57426-51239 N0 58416-2816 |  |  |  |  |  |  |  | 56 48 |  | dB dB |  |  |  | . V1 – IIW |  |  |  |  |  |  |  |  |  |  |  |  |  |
| #### RESULT |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| #### Name of sample |  | #### Test length, mm | #### Transducer Angle |  | #### Indication N0 |  |  |  |  | #### Leg |  |  | #### Decibel |  |  |  |  |  |  |  |  |  |  |  |  |  | #### Discontinuities |  |  |  |  |  |  |  |  |  |  |  | #### Assess to AWS D1.1:2015 |  |  | #### Remark |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | #### Indication level |  |  |  | #### Reference level |  | #### Attenuation factor |  |  |  | #### Indication rating |  |  |  | #### Length |  | #### Sound Path |  |  |  |  |  | #### Depth from A surface |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | #### a |  |  |  | #### b |  | #### c |  |  |  | #### d |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| #### P1 |  | #### 330 | #### 70 |  | #### - |  |  |  |  | #### - |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  |  |  | #### - |  |  |  | Accept |  |  |  |  |  |  |  |  |
| P2 |  | #### 165 | #### 70 |  | #### - |  |  |  |  | #### - |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  |  |  | #### - |  |  |  | Accept |  |  |  |  |  |  |  |  |
| P3 |  | 165 | #### 70 |  | #### - |  |  |  |  | #### - |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  |  |  | #### - |  |  |  | Accept |  |  |  |  |  |  |  |  |
| P4 |  | 330 | #### 70 |  | #### - |  |  |  |  | #### - |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  |  |  | #### - |  |  |  | Accept |  |  |  |  |  |  |  |  |
| Quatest3 12/07/2019 |  |  |  |  |  |  |  |  |  | Tested by |  |  |  |  |  |  |  |  |  |  |  |  | PT. Laboratory |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Vice Director |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  | Đào Công Huân |  |  |  |  |  |  |  |  |  |  |  | Nguyễn Văn Hồng Chi |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Nguyễn Thị Thủy |  |  |  |  |  |  |  |  |
| Name & dated signature |  |  |  |  |  |  |  |  |  | Name & dated signature |  |  |  |  |  |  |  |  |  |  |  |  | Name & dated signature |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Name & dated signature |  |  |  |  |  |  |  |  |  |

|  |  |  |  |  |  | CÔNG TY CỔ PHẦN TƯ VẤN KIỂM ĐỊNH XÂY DỰNG PHÍA NAM SOUTH CONTRUCTION ISPECTION CONSULTANT JSC |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Add: Phòng B01 – Tòa nhà ETUNNEL. L11 - L12 Miếu Nỗi, P. 13, Q. Bình Thạnh, Tp. Hồ Chí Minh. Mobil: (84) 8.35 123 171 – 35 170 334 – Fax: (84)8. 35 123 181. E-mail: scic@dmc.vn |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| NO: 00709-14 |  |  |  | BÁO CÁO KIỂM TRA SIÊU ÂM ULTRASONIC EXAMINATION REPORT |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Page : 01/01 |  |  |  |  |  |  |
| Project: VIETNAM NISSHIN TECHNOMIC PREMIX NEW FACTORY. |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Client: CÔNG TY TNHH QUỐC TẾ VINATA - CHI NHÁNH TP. HỒ CHÍ MINH. |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Test place: CÔNG TY CP CK XD TM ĐẠI DŨNG . |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Test method : AWS D1.1-2015 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Name of sample: AR10 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Date of testing: 08 & 10/07/2019 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | # Specification: AWS D1.1-2015 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| KETCH : |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| PREPARATION |  |  |  |  |  |  |  | SURFACE CONDITION |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | COUPLANT |  |  |  |  |  |  |  |  | MATERIAL |  |  |  |  |  |  |  |  |  |  |  |  |  |
| . Single V . Double V . Single V backing . Others |  |  |  |  |  |  |  | . Machined . Ground . Rolled |  |  |  |  |  |  |  |  |  | . One side . Both side . One surface . Both surface |  |  |  |  |  |  |  | . Water . Oil . Grease . Cellulose paste |  |  |  |  |  |  |  | . Carbon steel . Stainless steel |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | . Diameter : . W/ thickness |  |  |  |  |  | 8 |  |  | mm mm |  |  |  |  |
| UT INSTRUMENT |  |  |  |  |  |  |  |  |  |  |  |  |  | PROBE REFERENCE LEVEL |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | CALIBRATION BLOCKS |  |  |  |  |  |  |  |  |  |  |  |  |  |
| .GE USM 35 X DAC 13604a |  |  |  |  |  |  |  |  |  |  |  |  |  | . MSEB 4 00 . SWB 70-2E |  |  |  |  |  | N0 57426-51239 N0 58416-2816 |  |  |  |  |  |  |  | 56 48 |  | dB dB |  |  |  | . V1 – IIW |  |  |  |  |  |  |  |  |  |  |  |  |  |
| #### RESULT |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| #### Name of sample |  | #### Test length, mm | #### Transducer Angle |  | #### Indication N0 |  |  |  |  | #### Leg |  |  | #### Decibel |  |  |  |  |  |  |  |  |  |  |  |  |  | #### Discontinuities |  |  |  |  |  |  |  |  |  |  |  | #### Assess to AWS D1.1:2015 |  |  | #### Remark |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | #### Indication level |  |  |  | #### Reference level |  | #### Attenuation factor |  |  |  | #### Indication rating |  |  |  | #### Length |  | #### Sound Path |  |  |  |  |  | #### Depth from A surface |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | #### a |  |  |  | #### b |  | #### c |  |  |  | #### d |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| #### P1 |  | #### 330 | #### 70 |  | #### - |  |  |  |  | #### - |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  |  |  | #### - |  |  |  | Accept |  |  |  |  |  |  |  |  |
| P2 |  | #### 165 | #### 70 |  | #### - |  |  |  |  | #### - |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  |  |  | #### - |  |  |  | Accept |  |  |  |  |  |  |  |  |
| P3 |  | 330 | #### 70 |  | #### - |  |  |  |  | #### - |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  |  |  | #### - |  |  |  | Accept |  |  |  |  |  |  |  |  |
| Quatest3 12/07/2019 |  |  |  |  |  |  |  |  |  | Tested by |  |  |  |  |  |  |  |  |  |  |  |  | PT. Laboratory |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Vice Director |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  | Đào Công Huân |  |  |  |  |  |  |  |  |  |  |  | Nguyễn Văn Hồng Chi |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Nguyễn Thị Thủy |  |  |  |  |  |  |  |  |
| Name & dated signature |  |  |  |  |  |  |  |  |  | Name & dated signature |  |  |  |  |  |  |  |  |  |  |  |  | Name & dated signature |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Name & dated signature |  |  |  |  |  |  |  |  |  |

|  |  |  |  |  |  | CÔNG TY CỔ PHẦN TƯ VẤN KIỂM ĐỊNH XÂY DỰNG PHÍA NAM SOUTH CONTRUCTION ISPECTION CONSULTANT JSC |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Add: Phòng B01 – Tòa nhà ETUNNEL. L11 - L12 Miếu Nỗi, P. 13, Q. Bình Thạnh, Tp. Hồ Chí Minh. Mobil: (84) 8.35 123 171 – 35 170 334 – Fax: (84)8. 35 123 181. E-mail: scic@dmc.vn |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| NO: 00709-15 |  |  |  | BÁO CÁO KIỂM TRA SIÊU ÂM ULTRASONIC EXAMINATION REPORT |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Page : 01/01 |  |  |  |  |  |  |
| Project: VIETNAM NISSHIN TECHNOMIC PREMIX NEW FACTORY. |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Client: CÔNG TY TNHH QUỐC TẾ VINATA - CHI NHÁNH TP. HỒ CHÍ MINH. |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Test place: CÔNG TY CP CK XD TM ĐẠI DŨNG . |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Test method : AWS D1.1-2015 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Name of sample: AR9 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Date of testing: 08 & 10/07/2019 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | # Specification: AWS D1.1-2015 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| KETCH : |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| PREPARATION |  |  |  |  |  |  |  | SURFACE CONDITION |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | COUPLANT |  |  |  |  |  |  |  |  | MATERIAL |  |  |  |  |  |  |  |  |  |  |  |  |  |
| . Single V . Double V . Single V backing . Others |  |  |  |  |  |  |  | . Machined . Ground . Rolled |  |  |  |  |  |  |  |  |  | . One side . Both side . One surface . Both surface |  |  |  |  |  |  |  | . Water . Oil . Grease . Cellulose paste |  |  |  |  |  |  |  | . Carbon steel . Stainless steel |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | . Diameter : . W/ thickness |  |  |  |  |  | 8 |  |  | mm mm |  |  |  |  |
| UT INSTRUMENT |  |  |  |  |  |  |  |  |  |  |  |  |  | PROBE REFERENCE LEVEL |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | CALIBRATION BLOCKS |  |  |  |  |  |  |  |  |  |  |  |  |  |
| .GE USM 35 X DAC 13604a |  |  |  |  |  |  |  |  |  |  |  |  |  | . MSEB 4 00 . SWB 70-2E |  |  |  |  |  | N0 57426-51239 N0 58416-2816 |  |  |  |  |  |  |  | 56 48 |  | dB dB |  |  |  | . V1 – IIW |  |  |  |  |  |  |  |  |  |  |  |  |  |
| #### RESULT |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| #### Name of sample |  | #### Test length, mm | #### Transducer Angle |  | #### Indication N0 |  |  |  |  | #### Leg |  |  | #### Decibel |  |  |  |  |  |  |  |  |  |  |  |  |  | #### Discontinuities |  |  |  |  |  |  |  |  |  |  |  | #### Assess to AWS D1.1:2015 |  |  | #### Remark |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | #### Indication level |  |  |  | #### Reference level |  | #### Attenuation factor |  |  |  | #### Indication rating |  |  |  | #### Length |  | #### Sound Path |  |  |  |  |  | #### Depth from A surface |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | #### a |  |  |  | #### b |  | #### c |  |  |  | #### d |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| #### P1 |  | #### 330 | #### 70 |  | #### - |  |  |  |  | #### - |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  |  |  | #### - |  |  |  | Accept |  |  |  |  |  |  |  |  |
| P2 |  | #### 165 | #### 70 |  | #### - |  |  |  |  | #### - |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  |  |  | #### - |  |  |  | Accept |  |  |  |  |  |  |  |  |
| P3 |  | 165 | #### 70 |  | #### - |  |  |  |  | #### - |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  |  |  | #### - |  |  |  | Accept |  |  |  |  |  |  |  |  |
| P4 |  | 165 | #### 70 |  | #### - |  |  |  |  | #### - |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  |  |  | #### - |  |  |  | Accept |  |  |  |  |  |  |  |  |
| P5 |  | 165 | #### 70 |  | #### - |  |  |  |  | #### - |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  |  |  | #### - |  |  |  | Accept |  |  |  |  |  |  |  |  |
| P3 |  | 330 | #### 70 |  | #### - |  |  |  |  | #### - |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  |  |  | #### - |  |  |  | Accept |  |  |  |  |  |  |  |  |
| Quatest3 12/07/2019 |  |  |  |  |  |  |  |  |  | Tested by |  |  |  |  |  |  |  |  |  |  |  |  | PT. Laboratory |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Vice Director |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  | Đào Công Huân |  |  |  |  |  |  |  |  |  |  |  | Nguyễn Văn Hồng Chi |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Nguyễn Thị Thủy |  |  |  |  |  |  |  |  |
| Name & dated signature |  |  |  |  |  |  |  |  |  | Name & dated signature |  |  |  |  |  |  |  |  |  |  |  |  | Name & dated signature |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Name & dated signature |  |  |  |  |  |  |  |  |  |

|  |  |  |  |  |  | CÔNG TY CỔ PHẦN TƯ VẤN KIỂM ĐỊNH XÂY DỰNG PHÍA NAM SOUTH CONTRUCTION ISPECTION CONSULTANT JSC |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Add: Phòng B01 – Tòa nhà ETUNNEL. L11 - L12 Miếu Nỗi, P. 13, Q. Bình Thạnh, Tp. Hồ Chí Minh. Mobil: (84) 8.35 123 171 – 35 170 334 – Fax: (84)8. 35 123 181. E-mail: scic@dmc.vn |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| NO: 00709-16 |  |  |  | BÁO CÁO KIỂM TRA SIÊU ÂM ULTRASONIC EXAMINATION REPORT |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Page : 01/01 |  |  |  |  |  |  |
| Project: VIETNAM NISSHIN TECHNOMIC PREMIX NEW FACTORY. |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Client: CÔNG TY TNHH QUỐC TẾ VINATA - CHI NHÁNH TP. HỒ CHÍ MINH. |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Test place: CÔNG TY CP CK XD TM ĐẠI DŨNG . |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Test method : AWS D1.1-2015 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Name of sample: AC7 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Date of testing: 10/07/2019 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | # Specification: AWS D1.1-2015 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| KETCH : |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| PREPARATION |  |  |  |  |  |  |  | SURFACE CONDITION |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | COUPLANT |  |  |  |  |  |  |  |  | MATERIAL |  |  |  |  |  |  |  |  |  |  |  |  |  |
| . Single V . Double V . Single V backing . Others |  |  |  |  |  |  |  | . Machined . Ground . Rolled |  |  |  |  |  |  |  |  |  | . One side . Both side . One surface . Both surface |  |  |  |  |  |  |  | . Water . Oil . Grease . Cellulose paste |  |  |  |  |  |  |  | . Carbon steel . Stainless steel |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | . Diameter : . W/ thickness |  |  |  |  |  | 8 |  |  | mm mm |  |  |  |  |
| UT INSTRUMENT |  |  |  |  |  |  |  |  |  |  |  |  |  | PROBE REFERENCE LEVEL |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | CALIBRATION BLOCKS |  |  |  |  |  |  |  |  |  |  |  |  |  |
| .GE USM 35 X DAC 13604a |  |  |  |  |  |  |  |  |  |  |  |  |  | . MSEB 4 00 . SWB 70-2E |  |  |  |  |  | N0 57426-51239 N0 58416-2816 |  |  |  |  |  |  |  | 56 48 |  | dB dB |  |  |  | . V1 – IIW |  |  |  |  |  |  |  |  |  |  |  |  |  |
| #### RESULT |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| #### Name of sample |  | #### Test length, mm | #### Transducer Angle |  | #### Indication N0 |  |  |  |  | #### Leg |  |  | #### Decibel |  |  |  |  |  |  |  |  |  |  |  |  |  | #### Discontinuities |  |  |  |  |  |  |  |  |  |  |  | #### Assess to AWS D1.1:2015 |  |  | #### Remark |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | #### Indication level |  |  |  | #### Reference level |  | #### Attenuation factor |  |  |  | #### Indication rating |  |  |  | #### Length |  | #### Sound Path |  |  |  |  |  | #### Depth from A surface |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | #### a |  |  |  | #### b |  | #### c |  |  |  | #### d |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| #### P1 |  | #### 330 | #### 70 |  | #### - |  |  |  |  | #### - |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  |  |  | #### - |  |  |  | Accept |  |  |  |  |  |  |  |  |
| P2 |  | #### 330 | #### 70 |  | #### - |  |  |  |  | #### - |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  |  |  | #### - |  |  |  | Accept |  |  |  |  |  |  |  |  |
| Quatest3 12/07/2019 |  |  |  |  |  |  |  |  |  | Tested by |  |  |  |  |  |  |  |  |  |  |  |  | PT. Laboratory |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Vice Director |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  | Đào Công Huân |  |  |  |  |  |  |  |  |  |  |  | Nguyễn Văn Hồng Chi |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Nguyễn Thị Thủy |  |  |  |  |  |  |  |  |
| Name & dated signature |  |  |  |  |  |  |  |  |  | Name & dated signature |  |  |  |  |  |  |  |  |  |  |  |  | Name & dated signature |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Name & dated signature |  |  |  |  |  |  |  |  |  |

|  |  |  |  |  |  | CÔNG TY CỔ PHẦN TƯ VẤN KIỂM ĐỊNH XÂY DỰNG PHÍA NAM SOUTH CONTRUCTION ISPECTION CONSULTANT JSC |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Add: Phòng B01 – Tòa nhà ETUNNEL. L11 - L12 Miếu Nỗi, P. 13, Q. Bình Thạnh, Tp. Hồ Chí Minh. Mobil: (84) 8.35 123 171 – 35 170 334 – Fax: (84)8. 35 123 181. E-mail: scic@dmc.vn |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| NO: 00709-17 |  |  |  | BÁO CÁO KIỂM TRA SIÊU ÂM ULTRASONIC EXAMINATION REPORT |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Page : 01/01 |  |  |  |  |  |  |
| Project: VIETNAM NISSHIN TECHNOMIC PREMIX NEW FACTORY. |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Client: CÔNG TY TNHH QUỐC TẾ VINATA - CHI NHÁNH TP. HỒ CHÍ MINH. |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Test place: CÔNG TY CP CK XD TM ĐẠI DŨNG . |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Test method : AWS D1.1-2015 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Name of sample: AC4/1 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Date of testing: 10/07/2019 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | # Specification: AWS D1.1-2015 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| KETCH : |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| PREPARATION |  |  |  |  |  |  |  | SURFACE CONDITION |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | COUPLANT |  |  |  |  |  |  |  |  | MATERIAL |  |  |  |  |  |  |  |  |  |  |  |  |  |
| . Single V . Double V . Single V backing . Others |  |  |  |  |  |  |  | . Machined . Ground . Rolled |  |  |  |  |  |  |  |  |  | . One side . Both side . One surface . Both surface |  |  |  |  |  |  |  | . Water . Oil . Grease . Cellulose paste |  |  |  |  |  |  |  | . Carbon steel . Stainless steel |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | . Diameter : . W/ thickness |  |  |  |  |  | 8 |  |  | mm mm |  |  |  |  |
| UT INSTRUMENT |  |  |  |  |  |  |  |  |  |  |  |  |  | PROBE REFERENCE LEVEL |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | CALIBRATION BLOCKS |  |  |  |  |  |  |  |  |  |  |  |  |  |
| .GE USM 35 X DAC 13604a |  |  |  |  |  |  |  |  |  |  |  |  |  | . MSEB 4 00 . SWB 70-2E |  |  |  |  |  | N0 57426-51239 N0 58416-2816 |  |  |  |  |  |  |  | 56 48 |  | dB dB |  |  |  | . V1 – IIW |  |  |  |  |  |  |  |  |  |  |  |  |  |
| #### RESULT |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| #### Name of sample |  | #### Test length, mm | #### Transducer Angle |  | #### Indication N0 |  |  |  |  | #### Leg |  |  | #### Decibel |  |  |  |  |  |  |  |  |  |  |  |  |  | #### Discontinuities |  |  |  |  |  |  |  |  |  |  |  | #### Assess to AWS D1.1:2015 |  |  | #### Remark |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | #### Indication level |  |  |  | #### Reference level |  | #### Attenuation factor |  |  |  | #### Indication rating |  |  |  | #### Length |  | #### Sound Path |  |  |  |  |  | #### Depth from A surface |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | #### a |  |  |  | #### b |  | #### c |  |  |  | #### d |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| #### P1 |  | #### 330 | #### 70 |  | #### - |  |  |  |  | #### - |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  |  |  | #### - |  |  |  | Accept |  |  |  |  |  |  |  |  |
| P2 |  | #### 330 | #### 70 |  | #### - |  |  |  |  | #### - |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  |  |  | #### - |  |  |  | Accept |  |  |  |  |  |  |  |  |
| Quatest3 12/07/2019 |  |  |  |  |  |  |  |  |  | Tested by |  |  |  |  |  |  |  |  |  |  |  |  | PT. Laboratory |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Vice Director |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  | Đào Công Huân |  |  |  |  |  |  |  |  |  |  |  | Nguyễn Văn Hồng Chi |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Nguyễn Thị Thủy |  |  |  |  |  |  |  |  |
| Name & dated signature |  |  |  |  |  |  |  |  |  | Name & dated signature |  |  |  |  |  |  |  |  |  |  |  |  | Name & dated signature |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Name & dated signature |  |  |  |  |  |  |  |  |  |

|  |  |  |  |  |  | CÔNG TY CỔ PHẦN TƯ VẤN KIỂM ĐỊNH XÂY DỰNG PHÍA NAM SOUTH CONTRUCTION ISPECTION CONSULTANT JSC |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Add: Phòng B01 – Tòa nhà ETUNNEL. L11 - L12 Miếu Nỗi, P. 13, Q. Bình Thạnh, Tp. Hồ Chí Minh. Mobil: (84) 8.35 123 171 – 35 170 334 – Fax: (84)8. 35 123 181. E-mail: scic@dmc.vn |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| NO: 00709-18 |  |  |  | BÁO CÁO KIỂM TRA SIÊU ÂM ULTRASONIC EXAMINATION REPORT |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Page : 01/01 |  |  |  |  |  |  |
| Project: VIETNAM NISSHIN TECHNOMIC PREMIX NEW FACTORY. |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Client: CÔNG TY TNHH QUỐC TẾ VINATA - CHI NHÁNH TP. HỒ CHÍ MINH. |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Test place: CÔNG TY CP CK XD TM ĐẠI DŨNG . |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Test method : AWS D1.1-2015 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Name of sample: AC4/2 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Date of testing: 10/07/2019 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | # Specification: AWS D1.1-2015 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| KETCH : |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| PREPARATION |  |  |  |  |  |  |  | SURFACE CONDITION |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | COUPLANT |  |  |  |  |  |  |  |  | MATERIAL |  |  |  |  |  |  |  |  |  |  |  |  |  |
| . Single V . Double V . Single V backing . Others |  |  |  |  |  |  |  | . Machined . Ground . Rolled |  |  |  |  |  |  |  |  |  | . One side . Both side . One surface . Both surface |  |  |  |  |  |  |  | . Water . Oil . Grease . Cellulose paste |  |  |  |  |  |  |  | . Carbon steel . Stainless steel |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | . Diameter : . W/ thickness |  |  |  |  |  | 8 |  |  | mm mm |  |  |  |  |
| UT INSTRUMENT |  |  |  |  |  |  |  |  |  |  |  |  |  | PROBE REFERENCE LEVEL |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | CALIBRATION BLOCKS |  |  |  |  |  |  |  |  |  |  |  |  |  |
| .GE USM 35 X DAC 13604a |  |  |  |  |  |  |  |  |  |  |  |  |  | . MSEB 4 00 . SWB 70-2E |  |  |  |  |  | N0 57426-51239 N0 58416-2816 |  |  |  |  |  |  |  | 56 48 |  | dB dB |  |  |  | . V1 – IIW |  |  |  |  |  |  |  |  |  |  |  |  |  |
| #### RESULT |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| #### Name of sample |  | #### Test length, mm | #### Transducer Angle |  | #### Indication N0 |  |  |  |  | #### Leg |  |  | #### Decibel |  |  |  |  |  |  |  |  |  |  |  |  |  | #### Discontinuities |  |  |  |  |  |  |  |  |  |  |  | #### Assess to AWS D1.1:2015 |  |  | #### Remark |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | #### Indication level |  |  |  | #### Reference level |  | #### Attenuation factor |  |  |  | #### Indication rating |  |  |  | #### Length |  | #### Sound Path |  |  |  |  |  | #### Depth from A surface |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | #### a |  |  |  | #### b |  | #### c |  |  |  | #### d |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| #### P1 |  | #### 330 | #### 70 |  | #### - |  |  |  |  | #### - |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  |  |  | #### - |  |  |  | Accept |  |  |  |  |  |  |  |  |
| P2 |  | #### 330 | #### 70 |  | #### - |  |  |  |  | #### - |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  |  |  | #### - |  |  |  | Accept |  |  |  |  |  |  |  |  |
| Quatest3 12/07/2019 |  |  |  |  |  |  |  |  |  | Tested by |  |  |  |  |  |  |  |  |  |  |  |  | PT. Laboratory |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Vice Director |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  | Đào Công Huân |  |  |  |  |  |  |  |  |  |  |  | Nguyễn Văn Hồng Chi |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Nguyễn Thị Thủy |  |  |  |  |  |  |  |  |
| Name & dated signature |  |  |  |  |  |  |  |  |  | Name & dated signature |  |  |  |  |  |  |  |  |  |  |  |  | Name & dated signature |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Name & dated signature |  |  |  |  |  |  |  |  |  |

|  |  |  |  |  |  | CÔNG TY CỔ PHẦN TƯ VẤN KIỂM ĐỊNH XÂY DỰNG PHÍA NAM SOUTH CONTRUCTION ISPECTION CONSULTANT JSC |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Add: Phòng B01 – Tòa nhà ETUNNEL. L11 - L12 Miếu Nỗi, P. 13, Q. Bình Thạnh, Tp. Hồ Chí Minh. Mobil: (84) 8.35 123 171 – 35 170 334 – Fax: (84)8. 35 123 181. E-mail: scic@dmc.vn |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| NO: 00709-19 |  |  |  | BÁO CÁO KIỂM TRA SIÊU ÂM ULTRASONIC EXAMINATION REPORT |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Page : 01/01 |  |  |  |  |  |  |
| Project: VIETNAM NISSHIN TECHNOMIC PREMIX NEW FACTORY. |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Client: CÔNG TY TNHH QUỐC TẾ VINATA - CHI NHÁNH TP. HỒ CHÍ MINH. |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Test place: CÔNG TY CP CK XD TM ĐẠI DŨNG . |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Test method : AWS D1.1-2015 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Name of sample: AC4/3 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Date of testing: 10/07/2019 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | # Specification: AWS D1.1-2015 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| KETCH : |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| PREPARATION |  |  |  |  |  |  |  | SURFACE CONDITION |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | COUPLANT |  |  |  |  |  |  |  |  | MATERIAL |  |  |  |  |  |  |  |  |  |  |  |  |  |
| . Single V . Double V . Single V backing . Others |  |  |  |  |  |  |  | . Machined . Ground . Rolled |  |  |  |  |  |  |  |  |  | . One side . Both side . One surface . Both surface |  |  |  |  |  |  |  | . Water . Oil . Grease . Cellulose paste |  |  |  |  |  |  |  | . Carbon steel . Stainless steel |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | . Diameter : . W/ thickness |  |  |  |  |  | 8 |  |  | mm mm |  |  |  |  |
| UT INSTRUMENT |  |  |  |  |  |  |  |  |  |  |  |  |  | PROBE REFERENCE LEVEL |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | CALIBRATION BLOCKS |  |  |  |  |  |  |  |  |  |  |  |  |  |
| .GE USM 35 X DAC 13604a |  |  |  |  |  |  |  |  |  |  |  |  |  | . MSEB 4 00 . SWB 70-2E |  |  |  |  |  | N0 57426-51239 N0 58416-2816 |  |  |  |  |  |  |  | 56 48 |  | dB dB |  |  |  | . V1 – IIW |  |  |  |  |  |  |  |  |  |  |  |  |  |
| #### RESULT |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| #### Name of sample |  | #### Test length, mm | #### Transducer Angle |  | #### Indication N0 |  |  |  |  | #### Leg |  |  | #### Decibel |  |  |  |  |  |  |  |  |  |  |  |  |  | #### Discontinuities |  |  |  |  |  |  |  |  |  |  |  | #### Assess to AWS D1.1:2015 |  |  | #### Remark |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | #### Indication level |  |  |  | #### Reference level |  | #### Attenuation factor |  |  |  | #### Indication rating |  |  |  | #### Length |  | #### Sound Path |  |  |  |  |  | #### Depth from A surface |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | #### a |  |  |  | #### b |  | #### c |  |  |  | #### d |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| #### P1 |  | #### 330 | #### 70 |  | #### - |  |  |  |  | #### - |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  |  |  | #### - |  |  |  | Accept |  |  |  |  |  |  |  |  |
| P2 |  | #### 330 | #### 70 |  | #### - |  |  |  |  | #### - |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  |  |  | #### - |  |  |  | Accept |  |  |  |  |  |  |  |  |
| Quatest3 12/07/2019 |  |  |  |  |  |  |  |  |  | Tested by |  |  |  |  |  |  |  |  |  |  |  |  | PT. Laboratory |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Vice Director |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  | Đào Công Huân |  |  |  |  |  |  |  |  |  |  |  | Nguyễn Văn Hồng Chi |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Nguyễn Thị Thủy |  |  |  |  |  |  |  |  |
| Name & dated signature |  |  |  |  |  |  |  |  |  | Name & dated signature |  |  |  |  |  |  |  |  |  |  |  |  | Name & dated signature |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Name & dated signature |  |  |  |  |  |  |  |  |  |

|  |  |  |  |  |  | CÔNG TY CỔ PHẦN TƯ VẤN KIỂM ĐỊNH XÂY DỰNG PHÍA NAM SOUTH CONTRUCTION ISPECTION CONSULTANT JSC |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Add: Phòng B01 – Tòa nhà ETUNNEL. L11 - L12 Miếu Nỗi, P. 13, Q. Bình Thạnh, Tp. Hồ Chí Minh. Mobil: (84) 8.35 123 171 – 35 170 334 – Fax: (84)8. 35 123 181. E-mail: scic@dmc.vn |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| NO: 00709-20 |  |  |  | BÁO CÁO KIỂM TRA SIÊU ÂM ULTRASONIC EXAMINATION REPORT |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Page : 01/01 |  |  |  |  |  |  |
| Project: VIETNAM NISSHIN TECHNOMIC PREMIX NEW FACTORY. |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Client: CÔNG TY TNHH QUỐC TẾ VINATA - CHI NHÁNH TP. HỒ CHÍ MINH. |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Test place: CÔNG TY CP CK XD TM ĐẠI DŨNG . |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Test method : AWS D1.1-2015 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Name of sample: AC4/4 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Date of testing: 10/07/2019 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | # Specification: AWS D1.1-2015 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| KETCH : |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| PREPARATION |  |  |  |  |  |  |  | SURFACE CONDITION |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | COUPLANT |  |  |  |  |  |  |  |  | MATERIAL |  |  |  |  |  |  |  |  |  |  |  |  |  |
| . Single V . Double V . Single V backing . Others |  |  |  |  |  |  |  | . Machined . Ground . Rolled |  |  |  |  |  |  |  |  |  | . One side . Both side . One surface . Both surface |  |  |  |  |  |  |  | . Water . Oil . Grease . Cellulose paste |  |  |  |  |  |  |  | . Carbon steel . Stainless steel |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | . Diameter : . W/ thickness |  |  |  |  |  | 8 |  |  | mm mm |  |  |  |  |
| UT INSTRUMENT |  |  |  |  |  |  |  |  |  |  |  |  |  | PROBE REFERENCE LEVEL |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | CALIBRATION BLOCKS |  |  |  |  |  |  |  |  |  |  |  |  |  |
| .GE USM 35 X DAC 13604a |  |  |  |  |  |  |  |  |  |  |  |  |  | . MSEB 4 00 . SWB 70-2E |  |  |  |  |  | N0 57426-51239 N0 58416-2816 |  |  |  |  |  |  |  | 56 48 |  | dB dB |  |  |  | . V1 – IIW |  |  |  |  |  |  |  |  |  |  |  |  |  |
| #### RESULT |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| #### Name of sample |  | #### Test length, mm | #### Transducer Angle |  | #### Indication N0 |  |  |  |  | #### Leg |  |  | #### Decibel |  |  |  |  |  |  |  |  |  |  |  |  |  | #### Discontinuities |  |  |  |  |  |  |  |  |  |  |  | #### Assess to AWS D1.1:2015 |  |  | #### Remark |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | #### Indication level |  |  |  | #### Reference level |  | #### Attenuation factor |  |  |  | #### Indication rating |  |  |  | #### Length |  | #### Sound Path |  |  |  |  |  | #### Depth from A surface |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | #### a |  |  |  | #### b |  | #### c |  |  |  | #### d |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| #### P1 |  | #### 330 | #### 70 |  | #### - |  |  |  |  | #### - |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  |  |  | #### - |  |  |  | Accept |  |  |  |  |  |  |  |  |
| P2 |  | #### 330 | #### 70 |  | #### - |  |  |  |  | #### - |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  |  |  | #### - |  |  |  | Accept |  |  |  |  |  |  |  |  |
| Quatest3 12/07/2019 |  |  |  |  |  |  |  |  |  | Tested by |  |  |  |  |  |  |  |  |  |  |  |  | PT. Laboratory |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Vice Director |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  | Đào Công Huân |  |  |  |  |  |  |  |  |  |  |  | Nguyễn Văn Hồng Chi |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Nguyễn Thị Thủy |  |  |  |  |  |  |  |  |
| Name & dated signature |  |  |  |  |  |  |  |  |  | Name & dated signature |  |  |  |  |  |  |  |  |  |  |  |  | Name & dated signature |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Name & dated signature |  |  |  |  |  |  |  |  |  |

|  |  |  |  |  |  | CÔNG TY CỔ PHẦN TƯ VẤN KIỂM ĐỊNH XÂY DỰNG PHÍA NAM SOUTH CONTRUCTION ISPECTION CONSULTANT JSC |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Add: Phòng B01 – Tòa nhà ETUNNEL. L11 - L12 Miếu Nỗi, P. 13, Q. Bình Thạnh, Tp. Hồ Chí Minh. Mobil: (84) 8.35 123 171 – 35 170 334 – Fax: (84)8. 35 123 181. E-mail: scic@dmc.vn |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| NO: 00709-21 |  |  |  | BÁO CÁO KIỂM TRA SIÊU ÂM ULTRASONIC EXAMINATION REPORT |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Page : 01/01 |  |  |  |  |  |  |
| Project: VIETNAM NISSHIN TECHNOMIC PREMIX NEW FACTORY. |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Client: CÔNG TY TNHH QUỐC TẾ VINATA - CHI NHÁNH TP. HỒ CHÍ MINH. |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Test place: CÔNG TY CP CK XD TM ĐẠI DŨNG . |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Test method : AWS D1.1-2015 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Name of sample: AC4/5 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Date of testing: 10/07/2019 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | # Specification: AWS D1.1-2015 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| KETCH : |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| PREPARATION |  |  |  |  |  |  |  | SURFACE CONDITION |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | COUPLANT |  |  |  |  |  |  |  |  | MATERIAL |  |  |  |  |  |  |  |  |  |  |  |  |  |
| . Single V . Double V . Single V backing . Others |  |  |  |  |  |  |  | . Machined . Ground . Rolled |  |  |  |  |  |  |  |  |  | . One side . Both side . One surface . Both surface |  |  |  |  |  |  |  | . Water . Oil . Grease . Cellulose paste |  |  |  |  |  |  |  | . Carbon steel . Stainless steel |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | . Diameter : . W/ thickness |  |  |  |  |  | 8 |  |  | mm mm |  |  |  |  |
| UT INSTRUMENT |  |  |  |  |  |  |  |  |  |  |  |  |  | PROBE REFERENCE LEVEL |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | CALIBRATION BLOCKS |  |  |  |  |  |  |  |  |  |  |  |  |  |
| .GE USM 35 X DAC 13604a |  |  |  |  |  |  |  |  |  |  |  |  |  | . MSEB 4 00 . SWB 70-2E |  |  |  |  |  | N0 57426-51239 N0 58416-2816 |  |  |  |  |  |  |  | 56 48 |  | dB dB |  |  |  | . V1 – IIW |  |  |  |  |  |  |  |  |  |  |  |  |  |
| #### RESULT |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| #### Name of sample |  | #### Test length, mm | #### Transducer Angle |  | #### Indication N0 |  |  |  |  | #### Leg |  |  | #### Decibel |  |  |  |  |  |  |  |  |  |  |  |  |  | #### Discontinuities |  |  |  |  |  |  |  |  |  |  |  | #### Assess to AWS D1.1:2015 |  |  | #### Remark |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | #### Indication level |  |  |  | #### Reference level |  | #### Attenuation factor |  |  |  | #### Indication rating |  |  |  | #### Length |  | #### Sound Path |  |  |  |  |  | #### Depth from A surface |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | #### a |  |  |  | #### b |  | #### c |  |  |  | #### d |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| #### P1 |  | #### 330 | #### 70 |  | #### - |  |  |  |  | #### - |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  |  |  | #### - |  |  |  | Accept |  |  |  |  |  |  |  |  |
| P2 |  | #### 330 | #### 70 |  | #### - |  |  |  |  | #### - |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  |  |  | #### - |  |  |  | Accept |  |  |  |  |  |  |  |  |
| Quatest3 12/07/2019 |  |  |  |  |  |  |  |  |  | Tested by |  |  |  |  |  |  |  |  |  |  |  |  | PT. Laboratory |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Vice Director |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  | Đào Công Huân |  |  |  |  |  |  |  |  |  |  |  | Nguyễn Văn Hồng Chi |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Nguyễn Thị Thủy |  |  |  |  |  |  |  |  |
| Name & dated signature |  |  |  |  |  |  |  |  |  | Name & dated signature |  |  |  |  |  |  |  |  |  |  |  |  | Name & dated signature |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Name & dated signature |  |  |  |  |  |  |  |  |  |

|  |  |  |  |  |  | CÔNG TY CỔ PHẦN TƯ VẤN KIỂM ĐỊNH XÂY DỰNG PHÍA NAM SOUTH CONTRUCTION ISPECTION CONSULTANT JSC |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Add: Phòng B01 – Tòa nhà ETUNNEL. L11 - L12 Miếu Nỗi, P. 13, Q. Bình Thạnh, Tp. Hồ Chí Minh. Mobil: (84) 8.35 123 171 – 35 170 334 – Fax: (84)8. 35 123 181. E-mail: scic@dmc.vn |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| NO: 00709-22 |  |  |  | BÁO CÁO KIỂM TRA SIÊU ÂM ULTRASONIC EXAMINATION REPORT |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Page : 01/01 |  |  |  |  |  |  |
| Project: VIETNAM NISSHIN TECHNOMIC PREMIX NEW FACTORY. |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Client: CÔNG TY TNHH QUỐC TẾ VINATA - CHI NHÁNH TP. HỒ CHÍ MINH. |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Test place: CÔNG TY CP CK XD TM ĐẠI DŨNG . |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Test method : AWS D1.1-2015 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Name of sample: AC4/6 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Date of testing: 10/07/2019 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | # Specification: AWS D1.1-2015 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| KETCH : |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| PREPARATION |  |  |  |  |  |  |  | SURFACE CONDITION |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | COUPLANT |  |  |  |  |  |  |  |  | MATERIAL |  |  |  |  |  |  |  |  |  |  |  |  |  |
| . Single V . Double V . Single V backing . Others |  |  |  |  |  |  |  | . Machined . Ground . Rolled |  |  |  |  |  |  |  |  |  | . One side . Both side . One surface . Both surface |  |  |  |  |  |  |  | . Water . Oil . Grease . Cellulose paste |  |  |  |  |  |  |  | . Carbon steel . Stainless steel |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | . Diameter : . W/ thickness |  |  |  |  |  | 8 |  |  | mm mm |  |  |  |  |
| UT INSTRUMENT |  |  |  |  |  |  |  |  |  |  |  |  |  | PROBE REFERENCE LEVEL |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | CALIBRATION BLOCKS |  |  |  |  |  |  |  |  |  |  |  |  |  |
| .GE USM 35 X DAC 13604a |  |  |  |  |  |  |  |  |  |  |  |  |  | . MSEB 4 00 . SWB 70-2E |  |  |  |  |  | N0 57426-51239 N0 58416-2816 |  |  |  |  |  |  |  | 56 48 |  | dB dB |  |  |  | . V1 – IIW |  |  |  |  |  |  |  |  |  |  |  |  |  |
| #### RESULT |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| #### Name of sample |  | #### Test length, mm | #### Transducer Angle |  | #### Indication N0 |  |  |  |  | #### Leg |  |  | #### Decibel |  |  |  |  |  |  |  |  |  |  |  |  |  | #### Discontinuities |  |  |  |  |  |  |  |  |  |  |  | #### Assess to AWS D1.1:2015 |  |  | #### Remark |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | #### Indication level |  |  |  | #### Reference level |  | #### Attenuation factor |  |  |  | #### Indication rating |  |  |  | #### Length |  | #### Sound Path |  |  |  |  |  | #### Depth from A surface |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | #### a |  |  |  | #### b |  | #### c |  |  |  | #### d |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| #### P1 |  | #### 330 | #### 70 |  | #### - |  |  |  |  | #### - |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  |  |  | #### - |  |  |  | Accept |  |  |  |  |  |  |  |  |
| P2 |  | #### 330 | #### 70 |  | #### - |  |  |  |  | #### - |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  |  |  | #### - |  |  |  | Accept |  |  |  |  |  |  |  |  |
| Quatest3 12/07/2019 |  |  |  |  |  |  |  |  |  | Tested by |  |  |  |  |  |  |  |  |  |  |  |  | PT. Laboratory |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Vice Director |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  | Đào Công Huân |  |  |  |  |  |  |  |  |  |  |  | Nguyễn Văn Hồng Chi |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Nguyễn Thị Thủy |  |  |  |  |  |  |  |  |
| Name & dated signature |  |  |  |  |  |  |  |  |  | Name & dated signature |  |  |  |  |  |  |  |  |  |  |  |  | Name & dated signature |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Name & dated signature |  |  |  |  |  |  |  |  |  |

|  |  |  |  |  |  | CÔNG TY CỔ PHẦN TƯ VẤN KIỂM ĐỊNH XÂY DỰNG PHÍA NAM SOUTH CONTRUCTION ISPECTION CONSULTANT JSC |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Add: Phòng B01 – Tòa nhà ETUNNEL. L11 - L12 Miếu Nỗi, P. 13, Q. Bình Thạnh, Tp. Hồ Chí Minh. Mobil: (84) 8.35 123 171 – 35 170 334 – Fax: (84)8. 35 123 181. E-mail: scic@dmc.vn |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| NO: 00709-23 |  |  |  | BÁO CÁO KIỂM TRA SIÊU ÂM ULTRASONIC EXAMINATION REPORT |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Page : 01/01 |  |  |  |  |  |  |
| Project: VIETNAM NISSHIN TECHNOMIC PREMIX NEW FACTORY. |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Client: CÔNG TY TNHH QUỐC TẾ VINATA - CHI NHÁNH TP. HỒ CHÍ MINH. |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Test place: CÔNG TY CP CK XD TM ĐẠI DŨNG . |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Test method : AWS D1.1-2015 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Name of sample: AC5/1 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Date of testing: 10/07/2019 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | # Specification: AWS D1.1-2015 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| KETCH : |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| PREPARATION |  |  |  |  |  |  |  | SURFACE CONDITION |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | COUPLANT |  |  |  |  |  |  |  |  | MATERIAL |  |  |  |  |  |  |  |  |  |  |  |  |  |
| . Single V . Double V . Single V backing . Others |  |  |  |  |  |  |  | . Machined . Ground . Rolled |  |  |  |  |  |  |  |  |  | . One side . Both side . One surface . Both surface |  |  |  |  |  |  |  | . Water . Oil . Grease . Cellulose paste |  |  |  |  |  |  |  | . Carbon steel . Stainless steel |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | . Diameter : . W/ thickness |  |  |  |  |  | 8 |  |  | mm mm |  |  |  |  |
| UT INSTRUMENT |  |  |  |  |  |  |  |  |  |  |  |  |  | PROBE REFERENCE LEVEL |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | CALIBRATION BLOCKS |  |  |  |  |  |  |  |  |  |  |  |  |  |
| .GE USM 35 X DAC 13604a |  |  |  |  |  |  |  |  |  |  |  |  |  | . MSEB 4 00 . SWB 70-2E |  |  |  |  |  | N0 57426-51239 N0 58416-2816 |  |  |  |  |  |  |  | 56 48 |  | dB dB |  |  |  | . V1 – IIW |  |  |  |  |  |  |  |  |  |  |  |  |  |
| #### RESULT |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| #### Name of sample |  | #### Test length, mm | #### Transducer Angle |  | #### Indication N0 |  |  |  |  | #### Leg |  |  | #### Decibel |  |  |  |  |  |  |  |  |  |  |  |  |  | #### Discontinuities |  |  |  |  |  |  |  |  |  |  |  | #### Assess to AWS D1.1:2015 |  |  | #### Remark |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | #### Indication level |  |  |  | #### Reference level |  | #### Attenuation factor |  |  |  | #### Indication rating |  |  |  | #### Length |  | #### Sound Path |  |  |  |  |  | #### Depth from A surface |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | #### a |  |  |  | #### b |  | #### c |  |  |  | #### d |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| #### P1 |  | #### 330 | #### 70 |  | #### - |  |  |  |  | #### - |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  |  |  | #### - |  |  |  | Accept |  |  |  |  |  |  |  |  |
| P2 |  | #### 330 | #### 70 |  | #### - |  |  |  |  | #### - |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  |  |  | #### - |  |  |  | Accept |  |  |  |  |  |  |  |  |
| Quatest3 12/07/2019 |  |  |  |  |  |  |  |  |  | Tested by |  |  |  |  |  |  |  |  |  |  |  |  | PT. Laboratory |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Vice Director |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  | Đào Công Huân |  |  |  |  |  |  |  |  |  |  |  | Nguyễn Văn Hồng Chi |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Nguyễn Thị Thủy |  |  |  |  |  |  |  |  |
| Name & dated signature |  |  |  |  |  |  |  |  |  | Name & dated signature |  |  |  |  |  |  |  |  |  |  |  |  | Name & dated signature |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Name & dated signature |  |  |  |  |  |  |  |  |  |

|  |  |  |  |  |  | CÔNG TY CỔ PHẦN TƯ VẤN KIỂM ĐỊNH XÂY DỰNG PHÍA NAM SOUTH CONTRUCTION ISPECTION CONSULTANT JSC |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Add: Phòng B01 – Tòa nhà ETUNNEL. L11 - L12 Miếu Nỗi, P. 13, Q. Bình Thạnh, Tp. Hồ Chí Minh. Mobil: (84) 8.35 123 171 – 35 170 334 – Fax: (84)8. 35 123 181. E-mail: scic@dmc.vn |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| NO: 00709-24 |  |  |  | BÁO CÁO KIỂM TRA SIÊU ÂM ULTRASONIC EXAMINATION REPORT |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Page : 01/01 |  |  |  |  |  |  |
| Project: VIETNAM NISSHIN TECHNOMIC PREMIX NEW FACTORY. |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Client: CÔNG TY TNHH QUỐC TẾ VINATA - CHI NHÁNH TP. HỒ CHÍ MINH. |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Test place: CÔNG TY CP CK XD TM ĐẠI DŨNG . |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Test method : AWS D1.1-2015 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Name of sample: AC5/2 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Date of testing: 10/07/2019 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | # Specification: AWS D1.1-2015 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| KETCH : |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| PREPARATION |  |  |  |  |  |  |  | SURFACE CONDITION |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | COUPLANT |  |  |  |  |  |  |  |  | MATERIAL |  |  |  |  |  |  |  |  |  |  |  |  |  |
| . Single V . Double V . Single V backing . Others |  |  |  |  |  |  |  | . Machined . Ground . Rolled |  |  |  |  |  |  |  |  |  | . One side . Both side . One surface . Both surface |  |  |  |  |  |  |  | . Water . Oil . Grease . Cellulose paste |  |  |  |  |  |  |  | . Carbon steel . Stainless steel |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | . Diameter : . W/ thickness |  |  |  |  |  | 8 |  |  | mm mm |  |  |  |  |
| UT INSTRUMENT |  |  |  |  |  |  |  |  |  |  |  |  |  | PROBE REFERENCE LEVEL |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | CALIBRATION BLOCKS |  |  |  |  |  |  |  |  |  |  |  |  |  |
| .GE USM 35 X DAC 13604a |  |  |  |  |  |  |  |  |  |  |  |  |  | . MSEB 4 00 . SWB 70-2E |  |  |  |  |  | N0 57426-51239 N0 58416-2816 |  |  |  |  |  |  |  | 56 48 |  | dB dB |  |  |  | . V1 – IIW |  |  |  |  |  |  |  |  |  |  |  |  |  |
| #### RESULT |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| #### Name of sample |  | #### Test length, mm | #### Transducer Angle |  | #### Indication N0 |  |  |  |  | #### Leg |  |  | #### Decibel |  |  |  |  |  |  |  |  |  |  |  |  |  | #### Discontinuities |  |  |  |  |  |  |  |  |  |  |  | #### Assess to AWS D1.1:2015 |  |  | #### Remark |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | #### Indication level |  |  |  | #### Reference level |  | #### Attenuation factor |  |  |  | #### Indication rating |  |  |  | #### Length |  | #### Sound Path |  |  |  |  |  | #### Depth from A surface |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | #### a |  |  |  | #### b |  | #### c |  |  |  | #### d |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| #### P1 |  | #### 330 | #### 70 |  | #### - |  |  |  |  | #### - |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  |  |  | #### - |  |  |  | Accept |  |  |  |  |  |  |  |  |
| P2 |  | #### 330 | #### 70 |  | #### - |  |  |  |  | #### - |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  |  |  | #### - |  |  |  | Accept |  |  |  |  |  |  |  |  |
| Quatest3 12/07/2019 |  |  |  |  |  |  |  |  |  | Tested by |  |  |  |  |  |  |  |  |  |  |  |  | PT. Laboratory |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Vice Director |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  | Đào Công Huân |  |  |  |  |  |  |  |  |  |  |  | Nguyễn Văn Hồng Chi |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Nguyễn Thị Thủy |  |  |  |  |  |  |  |  |
| Name & dated signature |  |  |  |  |  |  |  |  |  | Name & dated signature |  |  |  |  |  |  |  |  |  |  |  |  | Name & dated signature |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Name & dated signature |  |  |  |  |  |  |  |  |  |

|  |  |  |  |  |  | CÔNG TY CỔ PHẦN TƯ VẤN KIỂM ĐỊNH XÂY DỰNG PHÍA NAM SOUTH CONTRUCTION ISPECTION CONSULTANT JSC |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Add: Phòng B01 – Tòa nhà ETUNNEL. L11 - L12 Miếu Nỗi, P. 13, Q. Bình Thạnh, Tp. Hồ Chí Minh. Mobil: (84) 8.35 123 171 – 35 170 334 – Fax: (84)8. 35 123 181. E-mail: scic@dmc.vn |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| NO: 00709-25 |  |  |  | BÁO CÁO KIỂM TRA SIÊU ÂM ULTRASONIC EXAMINATION REPORT |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Page : 01/01 |  |  |  |  |  |  |
| Project: VIETNAM NISSHIN TECHNOMIC PREMIX NEW FACTORY. |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Client: CÔNG TY TNHH QUỐC TẾ VINATA - CHI NHÁNH TP. HỒ CHÍ MINH. |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Test place: CÔNG TY CP CK XD TM ĐẠI DŨNG . |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Test method : AWS D1.1-2015 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Name of sample: AC6 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Date of testing: 10/07/2019 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | # Specification: AWS D1.1-2015 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| KETCH : |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| PREPARATION |  |  |  |  |  |  |  | SURFACE CONDITION |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | COUPLANT |  |  |  |  |  |  |  |  | MATERIAL |  |  |  |  |  |  |  |  |  |  |  |  |  |
| . Single V . Double V . Single V backing . Others |  |  |  |  |  |  |  | . Machined . Ground . Rolled |  |  |  |  |  |  |  |  |  | . One side . Both side . One surface . Both surface |  |  |  |  |  |  |  | . Water . Oil . Grease . Cellulose paste |  |  |  |  |  |  |  | . Carbon steel . Stainless steel |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | . Diameter : . W/ thickness |  |  |  |  |  | 8 |  |  | mm mm |  |  |  |  |
| UT INSTRUMENT |  |  |  |  |  |  |  |  |  |  |  |  |  | PROBE REFERENCE LEVEL |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | CALIBRATION BLOCKS |  |  |  |  |  |  |  |  |  |  |  |  |  |
| .GE USM 35 X DAC 13604a |  |  |  |  |  |  |  |  |  |  |  |  |  | . MSEB 4 00 . SWB 70-2E |  |  |  |  |  | N0 57426-51239 N0 58416-2816 |  |  |  |  |  |  |  | 56 48 |  | dB dB |  |  |  | . V1 – IIW |  |  |  |  |  |  |  |  |  |  |  |  |  |
| #### RESULT |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| #### Name of sample |  | #### Test length, mm | #### Transducer Angle |  | #### Indication N0 |  |  |  |  | #### Leg |  |  | #### Decibel |  |  |  |  |  |  |  |  |  |  |  |  |  | #### Discontinuities |  |  |  |  |  |  |  |  |  |  |  | #### Assess to AWS D1.1:2015 |  |  | #### Remark |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | #### Indication level |  |  |  | #### Reference level |  | #### Attenuation factor |  |  |  | #### Indication rating |  |  |  | #### Length |  | #### Sound Path |  |  |  |  |  | #### Depth from A surface |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | #### a |  |  |  | #### b |  | #### c |  |  |  | #### d |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| #### P1 |  | #### 330 | #### 70 |  | #### - |  |  |  |  | #### - |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  |  |  | #### - |  |  |  | Accept |  |  |  |  |  |  |  |  |
| P2 |  | #### 330 | #### 70 |  | #### - |  |  |  |  | #### - |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  | #### - |  |  |  | #### - |  | #### - |  |  |  |  |  | #### - |  |  |  | Accept |  |  |  |  |  |  |  |  |
| Quatest3 12/07/2019 |  |  |  |  |  |  |  |  |  | Tested by |  |  |  |  |  |  |  |  |  |  |  |  | PT. Laboratory |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Vice Director |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  | Đào Công Huân |  |  |  |  |  |  |  |  |  |  |  | Nguyễn Văn Hồng Chi |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Nguyễn Thị Thủy |  |  |  |  |  |  |  |  |
| Name & dated signature |  |  |  |  |  |  |  |  |  | Name & dated signature |  |  |  |  |  |  |  |  |  |  |  |  | Name & dated signature |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Name & dated signature |  |  |  |  |  |  |  |  |  |